## Slide 1: Electrodeposition Coating Simulation Based on Lab Experiments and Manufacturing Line Monitoring for Automotive Design
Yuki ONISHI (Institute of Science Tokyo)

## Slide 2: What is Electrodeposition (ED) ?
Most widely-used anti-rust base-coat methods for various metal products including auto carbodies.
Depositing coating film by applying direct electric current in a paint pool.
In the actual car manufacturing line, the carbodies are moving in the paint pool.
Relatively good at depositing a uniform film on complex shapes such as carbody.
Cathode
Anode
Paint
＋
＋
http://n-link.nissan.co.jp/

## Slide 3: What is Electrodeposition (ED) ?
Simplified Overview of the Entire Carbody Paint Shop
ED Oven
Degrease
Intermediate Oven
Intermediate Coat
Topcoat Oven
Top Coat
To Assembly Line
Sealing/Undercoat
Electrodeposition (ED)
Preparation
Base-coat
Intermediate -coat
Top-coat
We focus on this process.

## Slide 4: Impact of ED Process on Carbody Design
Undercarriages are exposed to severe corrosive environments.
ED film thickness must be above minimum over the entire surface of the undercarriages.
Some undercarriage parts (e.g., side sills) have bag-like structures with multiple plates.
It is necessary to drill many ED holes to allow the electric current to pass through in the paint pool.
Side Sill
https://www.goauto.ca/
∴ Carbody designers should understand and consider the ED process, including the location, size, and number of ED holes.
ED Hole

## Slide 5: Need for ED Simulation
ED holes are essential for corrosion protection, but they are NOT welcome for strength or stiffness.
Thus, the following conflict always occurs between carbody designers.
Designer in Corrosion Section
Designer in Strength/Stiffness Section
Fewer ED holes!
In such a case, ED simulation can resolve the conflict based on quantitative evidence data and lead to the optimal carbody design.
More ED holes!

## Slide 6: What is ED Simulation?
Actual ED Line Carbody Mesh
ED Simulation
Electrodes (Anodes)
Paint Pool
Carbodies w/ Motion
Total length: about 30 m
5 slices of a carbody mesh

## Slide 7: What is ED Simulation?
Mesh: 4-node tet (T4) mesh for complex carbody shape.
Motion: Overset mesh method
Outputs: Time-histories of Surface potential, Current density, Film thickness.
Governing equation: Electrostatic Laplace equation () in the paint pool domain.
Boundary conditions:
  Wall (insulation) BC，
  Anodic (electrode surface) BC,
  Cathodic (carbody surface) BC: ED constitutive models for film initiation / resistance / growth.
Need to identify them via lab experiments
Need for accurate FEM-T4
Need for validation before deployment

## Slide 8: Objective
Table of body contents:
Methods: ES-FEM, Lab Experiment, Actual Line Measurement
Results: Validation at an Actual Manufacturing Line
Summary
Development of a practical ED simulator using the next-gen FE formulation (ES-FEM) with the ED constitutive models based on lab experiments and its validation for actual manufacturing.

## Slide 9: Methods: ES-FEM, Lab Experiment, and Actual Line Measurement

## Slide 10: The next-gen FE formulation: ES-FEM
Edge-based Smoothed Finite Element Method (ES-FEM) is a relatively new FE formulation proposed in 2006 by Prof. G. R. Liu (the 1st plenary speaker of APCOM2025).
S-FEM is one the gradient/strain smoothing techniques.
ES-FEM is a method as if putting a Gauss point at each edge center.
For example, in a 2D triangular mesh:
Standard FEM
Edge-based S-FEM (ES-FEM)
The red area shows the domain for gradient smoothing.
Search
S-FEM wiki
G.R. Liu et al., CRC Press
Using ES-FEM-T4, a super-linear mesh convergence rate in electrostatic analyses is expected.

## Slide 11: Overview of Our ED Experiment Lab
Oven
Tank
Electric Balance
Control PC
Contant Temp. Water Circulator
Data Logger
Contant Temp. Water Bath
High Voltage Power Source
Water Rise Sink
Waste Tank
We have sufficient ED testing facilities in the central area of Tokyo!!
Digital Microscope
Film Thickness Meter
Water Quality Meter

## Slide 12: 3 Major Lab Tests
The one-plate test is used to identify the numerical ED constitutive models:
  Film initiation model,
  Film resistance model,
  Film growth model.
The other tests are used for the validation of the identified ED constitutive models.
One-Plate Test
4-Plate Box Test
Circulating Pool Test
All strongly non-linear models… It takes 200 tests at least.

## Slide 13: One of the Actual Line Monitoring Devices
Carbody Surface Potential Measurement Device
Hang this device in the middle of carbody.
Put electric probes on the carbody surface.
Let is sink in the paint pool to measure the electric potential during the ED process.
We can obtain the time-histories of electric potential on the carbody surface.
Getting time-history monitoring data is very important for the validation of a line simulator, in addition to the final state data.
Watertight Box
Data Logger
Battery
Copper Cable
connected to probes
Making real devices by yourself for actual manufacturing line is sometimes necessary to motivate factory engineers, even though you are a computational engineer.

## Slide 14: Result: Validation Test at an Actual Manufacturing Line

## Slide 15: Validation Test
●
●
●
●
●
Ch.2：Hood
Ch.4：Roof
Ch.3：Side Door
Ch.5：Side Sill
Ch.7：Back Door
Ch.6：Floor (not visible on this Fig.)
Outline
Measurement
A surface potential logging device with 6 probes was mounted on a car running on an actual ED line.
After baking, the film thickness was measured at the probe points.
Simulation (Same as the mesh convergence test.)
Half-body analysis (only right-hand side).
The entire line shape, carbody motion, and standard electrode conditions are input.
Surface potential time history and final film thickness at the 6 points are compared.
Measured 6 Points (Ch.2 - 7):

## Slide 16: Validation Test
Carbody Mesh with 4-node Tetrahedron
An ED simulation requires a mesh for the space around the carbody like CFD.
In contrast to CFD, an ED mesh should include the room space and many narrow spaces among plates (such as inside of the side sill).
5 slices of a carbody mesh
Animated slices of a carbody mesh from rear to front
# of Elements
25M for carbody
7M for pool
(32M in total)
CPU Cost 7 hours with AMD EPYC 9274F x 1, MPI/OpenMP Hybrid.

## Slide 17: Validation Test
Validation of Time-history of Surface Potential (Ch. 2 and 3)
The simulated surface potential is a little high because the degradation of the membranes of electrodes was not precisely simulated; yet, the results generally agree with measured data in practical accuracy.

## Slide 18: Validation Test
Validation of Time-history of Surface Potential (Ch. 4 and 5)
The simulated surface potential is a little high because the degradation of the membranes of electrodes was not precisely simulated; yet, the results generally agree with measured data in practical accuracy.

## Slide 19: Validation Test
Validation of Time-history of Surface Potential (Ch. 6 and 7)
The deposition delay at the floor, an inner part, is reproduced successfully.
The simulated surface potential is a little high because the degradation of the membranes of electrodes was not precisely simulated; yet, the results generally agree with measured data in practical accuracy.

## Slide 20: Validation Test
Validation of Final Film Thickness
Point | Measured () | Simulated () | Error ()
Ch.2: Hood | 20.1 | 21.4 | 
Ch.3: Side Door | 19.0 | 21.0 | 
Ch.4: Roof | 17.0 | 19.3 | 
Ch.5: Side Sill | 20.0 | 21.6 | 
Ch.6: Floor |  | 14.5 | 
Ch.7: Back Door | 23.0 | 20.3 | 
Point |  |  | 
Ch.2: Hood | 20.1 | 21.4 | 
Ch.3: Side Door | 19.0 | 21.0 | 
Ch.4: Roof | 17.0 | 19.3 | 
Ch.5: Side Sill | 20.0 | 21.6 | 
Ch.6: Floor |  | 14.5 | 
Ch.7: Back Door | 23.0 | 20.3 | 
Although there is still room for improvement in accuracy, the maximum error in film thickness is less than 3 , which is accurate enough for practical use.
The validation example presented here is from about 10 years ago.
Due to confidentiality reasons, we cannot disclose the latest results.

## Slide 21: Summary

## Slide 22: Summary
An electrodeposition (ED) simulator was developed.
The simulator adopts the next-gen FE formulation (ES-FEM) with 4-node tetrahedral meshes for complex carbody shapes.
A series of lab experiments are conducted to identify the ED constitutive models.
A novel device to measure the time-histories of electric potential on the carbody surface was developed and utilized in actual manufacturing lines.
A test on an actual manufacturing line validated the effectiveness of our ED simulator.
Our commercial ED simulator is already in practical use in major Japanese car companies.
If you are interested in our ED simulator, please check the website.
Thank you for your kind attention!
Search
edesfem