## Slide 1: A Meshfree Approach for Large Deformation Analysis in Thermal Nanoimprint
Yuki ONISHI and Kenji AMAYA
Tokyo Institute of Technology

## Slide 2: Background
Thermal nanoimprinting and micro hot embossing have been in industrialization stage.
Effective method for process design (temperature, pressure, time, etc.) is required.
  Current situation
  Repetitive experiments for process optimization.
  Repetitive experiments cost high!!
  Numerical simulation should help.
Final Goal
Establishment of numerical technique for thermal nanoimprint process optimization.

## Slide 3: Choice of Numerical Method
Choice1: Continuum or Molecular
  If the target size is over several tens of nms, the number of molecules is large enough to be modeled as a continuum.
  The problem is huge for MD.
Choise2: Solid or Fluid
  In thermal imprints, temperature is around Tg at most.
  Rheology effect can be consolidated in viscoelastic model.
Choise3: Meshfree or Mesh
  “Mesh”(=FEM) is usually used and has achievements.
  “Meshfree”(=SPH, EFGM, etc.) is expected to be a good method to treat extremely large deformation, but still under development and yet has no achievements.
  Most of the researches use FEM.

## Slide 4: Our Previous Work (Outline)
Finite element Analysis
  Geometric nonlinear (Large deformation)
  Material nonlinear (thermo-viscoelastic polymer)
  Contact nonlinear
  Quasi-static analysis
Mold
（rigid）
Polymer
(thermo-viscoelastic)
Onishi et al.,
JVST B (2008) etc.‏
FE analyses agreed
with experiments
in case of
line-and-space
up to AR=1

## Slide 5: Our Previous Work (Viscoelastic)
Generalized Maxwell Model
Ginf
Gn
1
n
G1
Ginf：Long-term shear modulus
G0=Ginf +∑Gi：
Instantaneous shear Modulus
1~n：Relaxation time
When a forced displacement x(t)=sin(t) applied at the temperature q,
reaction force f(t) become
G' ：Shear storage modulus
(same phase)
G’’ ：Shear loss modulus
(90o shifted)

## Slide 6: Our Previous Work (Material Test)
Uniaxial tension-compression tests at various temperatures and frequencies
heater
device：01dB-METRAVIB VA2000
frequency range：0.001～200(Hz)‏
load range：±100(N)‏
temperature range：-150～450(degC)‏

## Slide 7: Our Previous Work (Example2)
10sec
30sec
60sec

## Slide 8: Our Previous Work (Example2)
90sec
120sec

## Slide 9: Our Previous Work (Example1)

## Slide 10: Our Previous Work (Example2)
Simulated deformations of the line-and-space imprinting agreed with experiments.
30
60
90
120
0
20
40
60
80
100
120
140
160
0
Pressure Holding Time [sec.]
Pattern Height [mm]
Experiment
Simulation
10

## Slide 11: Our Previous Work (Summary)
Time evolutional deformation behavior was successfully simulated with FEM in cases of line-and-space patterning.
The thermo-viscoelastic constitutive model we chose was appropriate.
It has potential to simulate any deformation in thermal nanoimprintings.

## Slide 12: Objective
Our previous work hit the wall…
In practical applications, AR over 1 is not uncommon. (even AR>3 is usual.)
FEM cannot treat the extremely large deformation without adaptive meshing. (Adaptive meshing is difficult to implement.)
Objective
Development of a meshfree method for viscoelastic large deformation analysis
(utilize it for thermal nanoimprint process optimization in the future)
Hiral et. al

## Slide 13: Difference between FEM and Meshfree
Way of domain integration
  FEM (element base)
integration point
OK
BAD
concave
volumetric locking
node
BAD
Frequently happens
especially in case of
compression analysis
nearly
incompressible

## Slide 14: Difference between FEM and Meshfree
Way of domain integration
  Meshfree (collocation type) ---- SPH
  Meshfree (Petrov-Galerkin type) ---- MLPG
  Meshfree (Galerkin type) ---- EFGM
    background cell integration
    nodal integration
    stress point integration (SPI)
    (No standard formulation of SPI)
    *No element
  *Less locking
  *Fair integration accuracy
  *Requirement of stabilization
node
stress
point
close to FEM

## Slide 15: Robust MLS Approximation
IR
Moving Least Squares (MLS) to build shape function
Support radius
Weight function
IR
IR
(small)

## Slide 16: Update of SP States
Location
Volume
Vinitial：initial volume，F：deformation gradient
x: current location, S: set of nodes in the support,
f: shape function

## Slide 17: Viscoelastic Material Properties
material constants used in example analysis
instantaneous Young’s modulus（E0）： 9 GPa
instantaneous Poisson’s ratio（n0）： 0.333・・・
instantaneous shear modulus（G0）： 3.375 GPa
bulk modulus（K）： 9 GPa
dimensionless shear modulus（g）： 0.9
relaxation time（t）： 5 s
long-term Young’s modulus（E∞）： 1 GPa
long-term Poission’s ratio（n∞）： 0.481
long-term shear modulus(G∞): 0.3375 GPa
behavior at
room temperature
behavior
around Tg

## Slide 18: Bending of Cantilever
Static/Quasi-static, Plane strain
50x5 structured grid nodes
Concentrated force at right-top node
Compared to FEM(ABAQUS/Standard) with same node arrangements and selective reduced integration quadrangle elements
Elastic/Viscoelastic body
1m
0.1m
200 kN
Force
Time
1s
100s

## Slide 19: Bending of Cantilever (elastic)
Less than 1% error of displacement
No problem in elastic large deflection analysis
E=1GPa, n=0.49
ABAQUS/Standard Proposed Method

## Slide 20: Bending of Cantilever (viscoelastic)
ABAQUS/Standard Proposed Method
E0=9GPa, n0=0.333, Einf=1GPa, ninf=0.481

## Slide 21: Bending of Cantilever (viscoelastic)
2.5% error of displacement
Error decreases as dt decreases
Further improvement of time-advancing scheme is necessary

## Slide 22: Imprinting-like Analysis
Quasi-static, plane strain
Horizontal bounding for left and right side
Vertical bounding for bottom side
Enforced displacement for right half of top side toward downward with horizontal bounding
Unstructured grid with fineness and coarseness
0.6mm disp.
in 80s
1mm
1mm

## Slide 23: Imprinting-like Analysis (FEM)
Inappropriate deformation because of the locking under the corner

## Slide 24: Imprinting-like Analysis (FEM)

## Slide 25: Imprinting-like Analysis (animation)
An appropriate result was obtained.

## Slide 26: Summary & Future Work
Summary
  A Meshfree formulation of large deformation of viscoelastic body was proposed.
  It has fair accuracy in large deflation analysis.
  Appropriate result is obtained in imprinting-like analysis.
  Further modification is required to apply it to thermal nanoimprint simulation.
Future work
  Improvement of time advancing scheme
  Verification with experiments or FEM with adaptive meshing
  Insertion of additional nodes and SPs during analysis
  Contact analysis
  Cooling and demolding analysis

## Slide 27
Appendix

## Slide 28: SP Integration (initialization)
(currently) SPs are generated from FE meshes [Note] meshes are only for initialization!!!
Locate every SP in the middle edges
(Belytschko’s SP integration has master and slave SPs.)
Corresponding SP volume is calculated with meshes
：node
(has only x and u)
：stress point (SP)
(has x, T, E, E v, etc.)

## Slide 29: Integration Correction
Integration constraint
Integration correction (IC)
n: outward normal unit vector, A: correspoiding nodal area
JS: set of SPs that include node J in the support
determine g s so that modified y s satisfy reproducing constraints
including integration constraint

## Slide 30: Quasi-implicit Time Advancing
Start of time increment loop
  Start of Newton-Raphson loop
    update support, w, f, etc.
    calc f int. and K
    calc r = f int. -f ext.
    solve K du = r
    update node locations
    update SP locations
  End of Newton-Raphson loop
End of time increment loop
Typical fully-implicit time advancing

## Slide 31: Quasi-implicit Time Advancing
Start of time increment loop
  update support, w, f, etc.
  renew f virtual
  Start of Newton-Raphson loop
    update support, w, f, etc.
    calc f int. and K
    calc r = f int. -f ext. -f virtual
    solve K du = r
    update node locations
    update SP locations
  End of Newton-Raphson loop
End of time increment loop
Enforcement of temporal continuity of the mechanical equilibrium
Constant shape function in each Newton-Raphson loop

## Slide 32
FEM
  Integration points are pseudo-Lagrange points.
  Elements must be convex.
  1st order triangular element has volumetric locking.
Meshfree with BG cells
  Integration points are Euler points.
  Difficulties in treating free surfaces.
  Difficulties in convection of state quantities.
Meshfree without cells
  Integration points are Lagrange points.
  Difficulties in precise domain integration.

## Slide 33: Shear Behavior of Polymer
Generalized Maxwell Model
Ginf
Gn
1
n
G1
Ginf：Long-term shear modulus
G0=Ginf +∑Gi：
Instantaneous shear Modulus
1~n：Relaxation time
When a forced displacement x(t)=sin(t) applied at the temperature q,
reaction force f(t) become
G' ：Shear storage modulus
(same phase)
G’’ ：Shear loss modulus
(90o shifted)

## Slide 34: Constitutive Equation of Polymer
Constitutive equation
1)Volumetric Behavior
2)Shear Behavior
[P] : hydrostatic stress tensor K : bulk modulus
Evol: volumetric strain
[I]: identity tensor
[S]: deviatoric stress tensor
G0: instantaneous shear modulus (=Ginf +G1+ ... + Gn)
[E’]: deviatoric strain tensor
gi: ith dimensionless shear modulus
(=Gi/G0)
[Ev’]i: ith viscous strain tensor
Combining [P] and [S], We obtain stress tensor [T] as:

## Slide 35: Temperature Dependency of Polymer
WLF law (temperature-time conversion)
temperature increase
reduced time increase
WLF law
t: real time
t’: reduced time
qref, C1, C2: material constants

## Slide 36: Patch Test
Elastic body, Static, Plane-strain
Irregularly-arranged nodes and SPs
Displacement BC for every external nodes
：node
：stress point (SP)

## Slide 37: Patch Test (animation)

## Slide 38: Patch Test (result)
within 1% error of Mises stress
Proposed method passes the patch test