## Slide 1: Accurate electrodeposition simulation of automobile bodies with edge-based smoothed finite element method using 4-node tetrahedral meshes
Yuki ONISHI Tokyo Institute of Technology (Japan)

## Slide 2: What is Electrodeposition (ED) ?
Outline
Most widely-used anti-rust basecoat methods for various metal products including carbodies.
Depositing coating film by applying direct electric current in a paint pool.
Relatively good at depositing a uniform film on bodies in complex shape.
+
-
Cathode
Anode
Paint
＋
http://n-link.nissan.co.jp/
＋

## Slide 3: What is Electrodeposition (ED) ?
Overview of the Carbody Paint Shop
ED Oven
Degrease
Intermediate Oven
Intermediate Coat
Topcoat Oven
Top Coat
To Assembly Line
Sealing/Undercoat
Electrodeposition (ED)
Preparation
ED is responsible for the basecoat of a carbody.

## Slide 4: What is Electrodeposition (ED) ?
Photos of ED Process Line
1. Deposition process
2. Water rinse process
3. Baking process
We focus on this process.

## Slide 5: Importance of ED for Safety
Quiz. Is this car safe as when it was new?
No, because corrosion on the carbody severely damaged its structural health. (At worst, the engine may fall off.)
As corrosion progresses, the design strength/stiffness cannot be guaranteed, although safety tests (such as crash tests) are usually conducted using new cars without corrosion.
ED coating is important for automotive safety.
https://wd40.pk/

## Slide 6: Difficulty in ED for Carbodies
Undercarriages are exposed to severe corrosive environments, especially due to seawater or snow-melting chemicals.
Some undercarriage parts (such as a side sill) have bag-like complex structures with many ED holes.
It is not easy to deposit a required minimal thick film at the innermost faces of a bag-like structure, even for ED.
Carbody design must consider the difficulty in ED process.
Side Sill
https://www.goauto.ca/

## Slide 7: Need for ED Simulation
In a car company, this kind of battle may happens.
To resolve this battle,
Corrosion Section
Strength/Stiffness Section
More ED holes for safety!
Fewer ED holes for safety!
ED simulations are important to optimal car design as well as crash simulations for automotive safety.
Note that this is a fiction.

## Slide 8: What is ED Simulation?
Actual ED Line
ED Simulation
Electrodes (Anodes)
Paint Pool
Carbody w/ Motion
Total Length: 20~30 m
Paint Pool
Carbody with Motion
Electrodes (Anodes)
are reproduced in a computer.

## Slide 9: What is ED Simulation?
Governing Equation: Electrostatic Laplace equation () in the paint pool domain.
Boundary Condition (BC):
  Insulation BC,
  Anodic (electrode surface) BC,
  Cathodic (carbody surface) BC: Film resistance/growth constitutive model.
Outputs:
  Surface potential,
  Current density,
  Coated film thickness.

## Slide 10: Framework of ED Simulation
Framework for Solid Mechanics Simulation
2. Model Identification
(stress/strain curve)
3. Calculation
(FEM etc.)
1. Basic Tests
(Tensile test)
https://www.aandd.co.jp/adhome/products/test/rth_rti.html
2. Model Identification
(film resistance/growth)
3. Calculation
(FEM etc.)
1. Basic Tests
(one-plate tests)
Notes: 材料力学における数値計算のフレームワークと比較すると，このような対応になっています．
電着塗装基礎実験は材料力学における引張試験に相当します．
モデル同定や計算の流れは同様です．

## Slide 11: Meshing Issue 1
Issue 1: Impossible to make a good HEX mesh for carbodies.
An ED simulation requires a mesh for the space around the carbody like CFD.
In contrast to CFD, an ED mesh includes the room space and many narrow spaces among plates (such as side sills).
Sliced view of a carbody mesh

## Slide 12: Meshing Issue 1 (cont.)
The shape of a carbody is too complex to be discretized into a good HEX mesh.
The cutcell or snappy HEX meshing is basically not suitable for the geometry with many holes. ( Massive increase in DOF, Linear mesh convergence rate, Presence of hanging nodes or polyhedral cells, Inapplicable to solid dynamics, etc.)
Only the surface mesh is shown.

✗
TET meshes are preferable in ED simulation.
Zoom-in view of a carbody mesh

## Slide 13: Meshing Issue 2
Issue 2: Both the standard 4-node and 10-node tetrahedral elements are inconvenient.
4-node TET (T4) has poor accuracy with only a linear mesh convergence rate. FEM-T4 and FVM-T4 require very fine meshes to obtain accurate results.
10-node TET (T10) has good accuracy with a quadratic mesh convergence rate; however, T10 mesh requires massively large DOF to represent complex shapes without any kink of element shapes.

## Slide 14: Meshing Issue 2 (cont.)
If there is a small hole on a carbody, the surface mesh around the hole looks like…
✗ T10 w/ kink leads to severe accuracy loss.
✗ T10 w/o kink leads to a massive increase in DOF.
Carbody
Carbody
Hole
Hole
Carbody
Hole
T4 mesh
T10 mesh w/ kink
T10 mesh w/o kink
The standard T4 and T10 elements are both inconvenient for carbodies to achieve accurate simulation with minimal DOF.

## Slide 15: Motivation
By the way, …
The smoothed finite element method (S-FEM) has become popular in recent years as a next-generation high-performance FEM.
Especially, the edge-based S-FEM using T4 mesh (ES-FEM-T4) is known to achieve a superlinear mesh convergence rate even with T4 meshes.
Therefore, we expect that…
ES-FEM-T4 could be a solution for the meshing issues to achieve fast and accurate ED simulation.

## Slide 16: Objective
Table of body contents:
Formulation of ES-FEM-T4 in ED Simulation
Benchmark Analyses
Validation Analyses (for the ED Constitutive Model)
Summary
Development of ED simulator using ES-FEM-T4 for practical (fast & accurate) ED simulations.

## Slide 17: Formulation of ES-FEM-T4 in ED Simulation

## Slide 18: What is S-FEM?
The Smoothed finite element method (S-FEM) is a relatively new FE formulation proposed by Prof. G. R. Liu in 2006.
S-FEM is one of the strain smoothing techniques.
There are several types of classical S-FEMs, depending on the domains of strain smoothing.
For example in 2D triangular (T3) mesh:
Standard FEM
Edge-based S-FEM (ES-FEM)
Node-based S-FEM (NS-FEM)

## Slide 19: How popular is S-FEM?
Number of journal papers written in English whose title contains “smoothed finite element”:
(inquired at Google Scholar)
The attraction of S-FEM is expanding continuously.

## Slide 20: Applications of S-FEMs in Our Lab
Solid mechanics
Static Implicit Dynamic Explicit Viscous Implicit
Laplace Field
Electrodeposition (ED)

## Slide 21: Brief Formulation of ES-FEM
Let us consider two 3-node triangular (T3) elements in 2D.
Calculate at each element as usual.
Distribute to the connecting edge with an area weight and build .
Calculate current density and nodal internal current in each edge smoothing domain.
As if putting an integration point on each edge center
etc.

## Slide 22: Mathematical Formulation of ES-FEM
: Volume of the edge smoothing domain of Edge ,
.
B-matrix of Edge ,
[
is the set elements connected to Edge ,
is the volume of Element ,
“6” denotes the number of edges of a tetrahedron.
is the B-matrix of Element .

## Slide 23: Mathematical Formulation of ES-FEM
: Current density vector of Edge ,
[ .
Contribution of Edge for the internal current vector,
.
The total internal current vector,
.
is the electric conductivity (constant),
is the nodal potential vector related to Edge ,
is the set of all edges in the FE mesh.
That’s all. The formulation is quite simple!

## Slide 24: Characteristics of ES-FEM-T4
Advantage
Superlinear mesh convergence (as fast as 2nd-order elems.).
Same input file as FEM-T4.
No increase in DOF (nodal potentials only; easy to code).
Disadvantage
Longer assembling time of (~x2 of FEM-T4 w/ the same mesh).
Wider bandwidth in (~x3 of FEM-T4 w/ the same mesh).
No longer an independent T4 element.
FEM-T3 (Bandwidth: 7)
ES-FEM-T3 (Bandwidth: 13)
A node is referred by 6 elements, 7 nodes.
A node is referred by 12 edges, 12 elements, 13 nodes.

## Slide 25: Other 3 Key Features in ED Formulation
1. Moving Boundary
The overset mesh method using two meshes is adopted.
Each interfacial node of the active pool elements is tied in the active body elements with the multi-point constraint (MPC).
The classical method of Lagrange multiplier is used to satisfy the MPCs.
Inactive Elements
Active Body Elements
Active Pool Elements
Liquid Level

## Slide 26: Other 3 Key Features in ED Formulation
2. Iterative Matrix Solver
The minimum residual method (MINRES) with the point Jacobi preconditioner is adopted.
Electrostatic Laplace equation forms a symmetric matrix.
Matrix is indefinite due to the method of Lagrange multiplier used by the overset mesh method etc..
CG cannot solve symmetric indefinite systems without static condensation.
In contrast, MINRES can solve symmetric indefinite systems without static condensation. (Why is MINRES without static condensation not so popular?)

## Slide 27: Other 3 Key Features in ED Formulation
3. Treatment for Strong Nonlinear
The polarization curve for BC has an “S” shape.
The polarization curve (Robin BC) is ideally described with the Tafel eq..
In reality, H2 bubbles generated on cathode block the current, forming an “S” shaped polarization curve.
An “S” shape may cause infinite loops in the Newton-Raphson method.
The ED solver needs to introduce special treatments, such as cutback of ; yet, the loop count becomes a lot (~8 times) anyway.
Current Density, (A/m2)
Surface Potential, (V)
0
Given Anode BC
(as a constant )
Solution
Initial Guess
H2 bubbles cover up the cathode face and becomes an insulator.
Tafel Eq.
Infinite Loop

## Slide 28: Benchmark Analyses

## Slide 29: 4-Plate BOX Simulation
Outline
Imitating a bag-like structure such as a side sill in a carbody.
Film thickness on the innermost surface (G-Face) is the most important so as to guarantee corrosion protection.
The film thickness is evaluated with 4 different meshes for mesh validation using FEM-T4 and ES-FEM-T4.
Film Thickness Anim.
4 Plates forms 3 bags.
3rd bag is difficult to be deposited.
Photo of a BOX

## Slide 30: 4-Plate BOX Simulation
Overview of Meshes
3.2 mm Mesh Seed Size (31k T4 elem.)
0.8 mm Mesh Seed Size (169k T4 elem.)
1.6 mm Mesh Seed Size (65k T4 elem.)
0.4 mm Mesh Seed Size (716k T4 elem.)
Only the surface meshes are shown.

## Slide 31: 4-Plate BOX Simulation
Film Thickness on A-Face (outermost surface)
FEM results (dashed lines) have tiny errors due to mesh coarseness.
Mesh seed size

## Slide 32: 4-Plate BOX Simulation
Film Thickness on C-Face (surface in the 1st bag)
FEM results (dashed lines) have small errors due to mesh coarseness.
Mesh seed size

## Slide 33: 4-Plate BOX Simulation
Film Thickness on E-Face (surface in the 2nd bag)
FEM results (dashed lines) have medium errors due to mesh coarseness.
Mesh seed size

## Slide 34: 4-Plate BOX Simulation
Film Thickness on G-Face (innermost surface)
FEM results (dashed lines) have large errors due to mesh coarseness. Meanwhile, ES-FEM (solid lines) results have no such errors.
Mesh seed size

## Slide 35: 4-Plate BOX Simulation
Comparison of Mesh Convergence Rate on G-Face
FEM-T4 shows a linear convergence.
ES-FEM-T4 shows a quadratic convergence.
ES-FEM-T4 has much better mesh convergence rate than FEM-T4.
The result of ES-FEM with the finest mesh (0.4 mm) is used as the reference.
In Final thickness

## Slide 36: 4-Plate BOX Simulation
Comparison of Calculation Time
on a PC (only 1 CPU: Intel i9-9960X)
With the same mesh, ES-FEM is slower than FEM by x2.
For the same accuracy, ES-FEM is faster than FEM by x4.
Mesh Size | FEM-T4 | ES-FEM-T4
3.2 mm | 7 s | 10 s
1.6 mm | 8 s | 14 s
0.8 mm | 12 s | 26 s
0.4 mm | 41 s | 125 s
Comparable Accuracy
ES-FEM-T4 is supremely efficient in comparison to FEM-T4.

## Slide 37: Actual Line Simulation
Outline
Half-body analysis (only right-hand side).
Entire line shape, carbody motion, and electrode conditions are faithfully reproduced.
1000 timesteps in 300 s (i.e., average s).
The film thickness is evaluated with 3 different meshes for mesh validation using FEM-T4 and ES-FEM-T4.

## Slide 38: Actual Line Simulation
Overview of Surface Mesh of 10M Element Mesh
There are many ED holes around narrow spaces among plates.
Only the surface mesh is shown.

## Slide 39: Actual Line Simulation
Overview of Surface Mesh of 16M Element Mesh
There are many ED holes around narrow spaces among plates.
Only the surface mesh is shown.

## Slide 40: Actual Line Simulation
Overview of Surface Mesh of 51M Element Mesh
There are many ED holes around narrow spaces among plates.
The difference in the mesh can be seen clearly by zooming in around a hole.
Only the surface mesh is shown.
Let’s zoom in here.

## Slide 41: Actual Line Simulation
Zoom in View around a Hole on Carbody
There are many ED holes around narrow spaces among plates.
The difference in the mesh can be seen clearly by zooming in around a hole.
10M
16M
51M
Coarse Dense

## Slide 42: Actual Line Simulation
Reference Solution of (ES-FEM with 51M Elems.)
Outer View Inner View

## Slide 43: Actual Line Simulation
Reference Solution of (ES-FEM with 51M Elems.)
Outer View Inner View

## Slide 44: Actual Line Simulation
Reference Solution of (ES-FEM with 51M Elems.)
Outer View Inner View

## Slide 45: Actual Line Simulation
Film Thickness Distribution with 51M Elem. Mesh
(Clipped View on Side Sill)
FEM shows a little thicker result. (The center of the side sill is Yellow.)
The ES-FEM result is regarded as a reference solution. (The center of the side sill is Green.)
FEM-T4
ES-FEM-T4
Reference Solution

## Slide 46: Actual Line Simulation
Film Thickness Distribution with 16M Elem. Mesh
(Clipped View on Side Sill)
FEM shows a much thicker result. (The center of the side sill is Orange.)
ES-FEM shows a similar result. (The center of the side sill is Green.)
FEM-T4
ES-FEM-T4

## Slide 47: Actual Line Simulation
Film Thickness Distribution with 10M Elem. Mesh
(Clipped View on Side Sill)
FEM shows a massively thicker result. (The center of the side sill is Red.)
ES-FEM shows a little thicker result. (The center of the side sill is Yellow.)
FEM-T4
ES-FEM-T4
Hard to be deposited but important point for anti-corrosion.
Let’s compare the time history of film thickness at a certain point.

## Slide 48: Actual Line Simulation
Comparison of Time-histories of Film Thickness
FEM-T4 with 51M elems. and ES-FEM-T4 with 10M elems. has almost comparable accuracy.
ES-FEM-T4 almost gets mesh converges with 16M elems. .

## Slide 49: Actual Line Simulation
Calculation Time
On a cluster (TSUBAME3.0: Intel Xeon E5-2680 v4, using 64 CPUs)
With the same mesh, ES-FEM is slower than FEM by x1.5.
For the same accuracy, ES-FEM is faster than FEM by x3.
# of Elements | FEM-T4 | ES-FEM-T4
10M | 1.6 h | 1.9 h
16M | 2.3 h | 3.4 h
51M | 6.0 h | 8.5 h
Comparable Accuracy
For accurate ED simulations, ES-FEM-T4 is much better than FEM-T4.

## Slide 50: Actual line Simulation
Strong Scaling Test (with 10M Elem. Mesh)
On a cluster (TSUBAME3.0: Intel Xeon E5-2680 v4)
  Some tasks, including MPCs for the moving boundary, are not yet fully parallelized (our future work).
Our ES-FEM code scales to some extent up to 64 CPUs at least.

## Slide 51: Validation Analyses (for the ED Constitutive Model)

## Slide 52: Framework of ED Simulation
Framework for Solid Mechanics Simulation
2. Model Identification
(stress/strain curve)
3. Calculation
(FEM etc.)
1. Basic Tests
(Tensile test)
https://www.aandd.co.jp/adhome/products/test/rth_rti.html
2. Model Identification
(film resistance/growth)
3. Calculation
(FEM etc.)
1. Basic Tests
(one-plate tests)
Notes: 材料力学における数値計算のフレームワークと比較すると，このような対応になっています．
電着塗装基礎実験は材料力学における引張試験に相当します．
モデル同定や計算の流れは同様です．

## Slide 53: Two Complexities in ED Phenomena
There are two nonlinearities in ED phenomena, thus our ED boundary model consists of 2 sub-models:
  Film resistance model Film resistance is NOT linear to film thickness :
: resistance, : const., : film thickness.
  Film growth model Film growth rate is NOT linear to current density :
: film growth rate, : const., : current density.
We need to conduct many lab tests to reveal these nonlinear behavior.

## Slide 54: Outline of the One-Plate Test
One plate is dipped in paint contained in a cylindrical anode.
Many tests are conducted with various applied voltages, deposition times, and stirring speed: about 150 tests in total. ( In-situ measurement of film thickness is impossible.)
Paint
Plate
Cylindical Container (Anode)
Stirred with Magnetic Stirrer
Input | Applied Voltage, Deposition Time, Stirring Speed (on/off).
Output | Time history of Current, Film thickness after Deposition.
Time (s)
Applied Voltage (V)

## Slide 55: Procedure to Identify Film Resistance Model
1. One-plate tests.
Plot
Data Fitting
2. Scatter diagram among .
3. Approximated surface for the resistance model.

## Slide 56: Procedure to Identify Film Growth Model
1. One-plate tests.
Plot
Data Fitting
Diffusive current density represents the amount of electricity consumed for the electrolysis of water (H2O), not used for the deposition of the coating film.
3. Approximated surface for the growth model.
2. Scatter diagram among

## Slide 57: One-Plate Test/Simulation
Comparison of Surface Potential Time Histories
The simulation curves agree well with the experimental ones with small error in the results at lower voltages.
Stirred (with Flow) Unstirred (without Flow)

## Slide 58: One-Plate Test/Simulation
Comparison of Current Density Time Histories
Stirred (with Flow) Unstirred (without Flow)
The simulation curves agree well with the experimental ones with small error in the results at lower voltages.

## Slide 59: One-Plate Test/Simulation
Comparison of Film Thickness Time Histories
Stirred (with Flow) Unstirred (without Flow)
The simulation curves agree well with the experimental ones with small error in the results at lower voltages.

## Slide 60: 4-Plate BOX Test/Simulation
Outline
Model for stirred BC is assigned to the outer surface, while that for unstirred BC is assigned to the other inner surfaces.
Accuracy of surface potential and final film thickness at the measurement points are evaluated using ES-FEM-T4.
Film Thickness
(http://plaza.rakuten.co.jp/heroc)
Side Sill

## Slide 61: 4-Plate BOX Simulation
Photo of the 4-Plate BOX Test
Paint
BOX
Thermostatic Bath
Container (Anode)

## Slide 62: 4-Plate BOX Test/Simulation
Comparison of Surface Potential Time Histories
The simulation curves agree well with the experimental ones.

## Slide 63: 4-Plate BOX Test/Simulation
Comparison of Current Density Time Histories
The simulation curves agree well with the experimental ones.

## Slide 64: 4-Plate BOX Test/Simulation
Comparison of Film Thickness Time Histories
Further improvement of the ED constitutive model is required.
The simulation curves agree well with the experimental ones, except the curve on the innermost face (G-Face): error.

## Slide 65: Actual Line Test/Simulation
Overview Six Measurement Points
Half-body analysis (only right-hand side).
Entire line shape, carbody motion, and electrode conditions are faithfully reproduced.
Model for stirred BC is assigned to the outer surface, while that for unstirred BC is assigned to the inner surface.
Accuracy of surface potential and final film thickness at the measurement points are evaluated using ES-FEM-T4.
●
●
●
●
●
Ch.2：Hood
Ch.4：Roof
Ch.3：Side Door
Ch.5：Side Sill
Ch.7：Back Door
Ch.6：Floor

## Slide 66: Actual Line Test/Simulation
Time History of Applied Voltage to Anodes
“Stage 1” denotes anodes on the entry side, whereas “Stage 2” denotes anodes on the exit side.
Note that there is a sudden turn on/off of power.
Stage 1
Stage 2

## Slide 67: Actual Line Test/Simulation
Comparison of Surface Potential Time Histories
Although the rise in surface potential tends to be faster in the simulation, the measurement curves are nearly reproduced.

## Slide 68: Actual Line Test/Simulation
Comparison of Surface Potential Time Histories
Although the rise in surface potential tends to be faster in the simulation, the measurement curves are nearly reproduced.

## Slide 69: Actual Line Test/Simulation
Comparison of Surface Potential Time Histories
The measurement results are reproduced with good accuracy even for inner plates (Ch.6: Floor), where lack of accuracy has been an issue.

## Slide 70: Actual Line Test/Simulation
Comparison of Final Film Thickness
Point | Measued () | Simulated () | Error ()
Ch.2: Hood | 20.1 | 21.4 | 
Ch.3: Side Door | 19.0 | 21.0 | 
Ch.4: Roof | 17.0 | 19.3 | 
Ch.5: Side Sill | 20.0 | 21.6 | 
Ch.6: Floor |  | 14.5 | 
Ch.7: Back Door | 23.0 | 20.3 | 
Point |  |  | 
Ch.2: Hood | 20.1 | 21.4 | 
Ch.3: Side Door | 19.0 | 21.0 | 
Ch.4: Roof | 17.0 | 19.3 | 
Ch.5: Side Sill | 20.0 | 21.6 | 
Ch.6: Floor |  | 14.5 | 
Ch.7: Back Door | 23.0 | 20.3 | 
The maximum error is less than , and thus our ED constitutive model has practical accuracy in the actual line simulation.

## Slide 71: Summary

## Slide 72: Summary
Conclusion
ES-FEM-T4 was applied to the actual ED line simulations.
The high accuracy of ES-FEM-T4, owing to its superlinear (almost quadratic) mesh convergence rate in ED simulation, was confirmed compared to the poor accuracy of FEM-T4.
Our parallelized ES-FEM-T4 code enabled us to obtain mesh-converged accurate solutions of actual line simulations in reasonable time with relatively coarse meshes.
Future Works
Improvement of the ED resistance/growth models.
Further validation of the ED models on the actual lines.
Take-home Message: Why don’t you us ES-FEM-T4?
Thank you for your kind attention.

## Slide 73
Appendix

## Slide 74: Pre-processes for ED Simulation
Mesh generation for body & pool.
Classification of body surfaces into inner & outer parts to assign different BCs (with/without stirring BC).
Mesh partitioning & reordering for MPI parallelization.
Preparation of input file including body motion definition.
Send to ED Solver

## Slide 75: Mechanism of Electrodeposition
Paint cations (“+” ions) are attracted to the cathode.
Paint ions gradually lose their electrical charge and are aggregated into paint particles.
Some of the paint particles are deposited as coating film. Meanwhile, the rests are diffused and re-dissolved.
In contrast to a simple electroplating, accurate numerical simulation of ED film thickness is quite difficult.
-
+
+
-
Paint Ions
Carbody
（Cathode)
-
-
+
Deposition
Aggregated into paint particles
When the particle gets big enough
Voltage is applied
Coating
Film
Electrophoresis

## Slide 76: What is ED Simulation ?
ED simulation provides film thickness, surface potential, surface current density and so on.
Film Thickness
Surface Potential
Surface Current Density
You can see that the paint film starts to be deposited from the outside surface.

## Slide 77: ED Boundary Models
Film Growth Model
It represents the relation between ．
Used to decide film growth rate.
After deposition ：
Film Resistance Model
It represents the relation between ．
Used to decide film resistance.
Flow rate dependency is considered．