## Slide 1: Automotive Electrodeposition Coating Simulation using Edge-based Smoothed Finite Element Method
Yuki ONISHI (Institute of Science Tokyo)

## Slide 2: Relatively Long Introduction to Electrodeposition Simulation

## Slide 3: What is Electrodeposition (ED) ?
Most widely-used anti-rust base-coat methods for various metal products including auto carbodies.
Depositing coating film by applying direct electric current in a paint pool.
In the actual car manufacturing line, the carbodies are moving in the paint pool.
Relatively good at depositing a uniform film on complex shapes such as carbody.
Cathode
Anode
Paint
＋
＋
http://n-link.nissan.co.jp/

## Slide 4: What is Electrodeposition (ED) ?
Simplified Overview of the Entire Carbody Paint Shop
ED Oven
Degrease
Intermediate Oven
Intermediate Coat
Topcoat Oven
Top Coat
To Assembly Line
Sealing/Undercoat
Electrodeposition (ED)
Preparation
Base-coat
Intermediate -coat
Top-coat
We focus on this process.

## Slide 5: Importance of ED for safety
No, because corrosion significantly reduces the strength and stiffness of a car.
As corrosion progresses, the initial strength and stiffness cannot be guaranteed.
Nevertheless, the safety inspections of cars (e.g., crash tests) are usually performed with new cars without corrosion……
ED is quite important for ensuring the long-term safety of carbodies.
https://wd40.pk/
Quiz.) Is this car safe as when it was new?

## Slide 6: Impact of ED process on carbody design
Undercarriages are exposed to severe corrosive environments.
ED film thickness must be above minimum over the entire surface of the undercarriages.
Some undercarriage parts (e.g., side sills) have bag-like structures with multiple plates.
It is necessary to drill many ED holes to allow the electric current to pass through in the paint pool.
Side Sill
https://www.goauto.ca/
∴ Carbody designers should understand and consider the ED process, including the location, size, and number of ED holes.
ED Hole

## Slide 7: Need for ED Simulation
ED holes are essential for corrosion protection, but they are NOT welcome for strength or stiffness.
Thus, the following conflict always occurs between carbody designers.
Designer in Corrosion Section
Designer in Strength/Stiffness Section
Fewer ED holes for safety!
In such a case, ED simulation can resolve the conflict based on quantitative evidence data and lead to the optimal carbody design.
More ED holes for safety!

## Slide 8: What is ED Simulation?
Actual ED Line
ED Simulation
Electrodes (Anodes)
Paint Pool
Carbodies w/ Motion
Total length: about 30 m
Paint Pool
Carbodies with Motion
Electrodes (Anodes)
are reproduced in a computer.

## Slide 9: What is ED Simulation?
Governing equation: Electrostatic Laplace equation () in the paint pool domain.
Boundary conditions:
  Wall (insulation) BC，
  Anodic (electrode surface) BC,
  Cathodic (carbody surface) BC: Film initiation/growth/resistance constitutive models.
Outputs: Time-histories of
  Surface potential,
  Current density,
  Film thickness
Identified via lab experiments.
Final film thickness is the main output.
Motion: Overset mesh method

## Slide 10: Two Issues in Meshing for ED Simulation
Issue #1: Impossible to make a good HEX mesh for carbodies.
An ED simulation requires a mesh for the space around the carbody like CFD.
In contrast to CFD, an ED mesh should include the room space and many narrow spaces among plates (such as inside of the side sill).
5 slices of a carbody mesh
Animated slices of a carbody mesh from rear to front

## Slide 11: Two Issues in Meshing for ED Simulation
The shape of a carbody is too complex to be discretized into a good HEX mesh.
The Cartesian mesh (e.g., cutcell mesh, snappy hex mesh, cube mesh) is basically NOT suitable for the geometry with many holes. ( Massive increase in DOF, Linear mesh convergence rate of H8 element, Presence of hanging nodes or polyhedral cells)

✗
TET meshes are preferable in ED simulation.
Zoom-in view of a carbody surface mesh

## Slide 12: Two Issues in Meshing for ED Simulation
Issue #2: Both the standard 4-node and 10-node tetrahedral elements are inconvenient.
4-node TET (T4) has poor accuracy with only a linear mesh convergence rate. FEM-T4 and FVM-T4 require very fine meshes to obtain accurate results.
10-node TET (T10) has good accuracy with a quadratic mesh convergence rate; however, T10 mesh requires a massively large DOF to represent complex shapes without any kink in element shapes.
T4
T10

## Slide 13: Two Issues in Meshing for ED Simulation
If there is a small hole on a carbody plate, the surface mesh around the hole looks like…
Both the standard T4 and T10 elements are inconvenient as a carbody mesh to achieve accurate simulation with minimal DOF.
Plate
Hole
T10 mesh w/ kink
✗ leads to severe accuracy loss in shape function with FEM-T10.
Plate
Hole
T10 mesh w/o kink
✗ leads to a massive increase in DOF with mid-nodes.
Plate
Hole
T4 mesh
✗ leads to poor mesh convergence rate with FEM-T4.
T4
T10

## Slide 14: Motivation
By the way, …
The smoothed finite element method (S-FEM) [detail later] has become popular in recent years as a next-generation high-performance FEM.
Especially, the edge-based S-FEM using T4 mesh (ES-FEM-T4) is known to achieve a superlinear mesh convergence rate even with T4 meshes.
Therefore, we expect that…
ES-FEM-T4 could be a solution for the meshing issues to achieve fast and accurate ED simulation.

## Slide 15: Objective
Table of body contents:
Quick Introduction to S-FEM
Mesh Convergence Test
Validation Test
Summary
Development of ED simulator using ES-FEM-T4 for practical (fast & accurate) ED simulations.

## Slide 16: Quick Introduction to Smoothed Finite Element Method (S-FEM)

## Slide 17: What is S-FEM?
Smoothed finite element method (S-FEM) is a relatively new FE formulation proposed in 2006.
S-FEM is one of the gradient (strain) smoothing techniques.
Many types of S-FEMs have been developed with various smoothing schemes.
There are a few classical S-FEMs depending on the smoothing domain.
For example, in a 2D triangular mesh:
Standard FEM
Edge-based S-FEM (ES-FEM)
Node-based S-FEM (NS-FEM)
Each colored area shows the domain for gradient smoothing.

## Slide 18: Brief of ES-FEM in Linear Elastic Analysis
Let us consider a mesh with only two 3-node triangular cells.
Make at each cell as usual.
At each edge, gather s of the connecting cells and average them with area weights to build .
Calculate strain , stress () and nodal internal force in each edge smoothing domain with .
As if putting a Gauss point at each edge center
etc.
Let me explain in 2D for simplicity
No shear locking.

## Slide 19: Performance of ES-FEM in Linear Elastic Analysis
Cantilever Bending Analysis with Dead Load at the Tip Size:10x1 m,
Mises stress
Pressure
ABAQUS CPE3 (Standard FEM-T3)
ES-FEM-T3
ES-FEM-T3 gives more accurate stress/strain distributions than the standard FEM-T3 using the same mesh.

## Slide 20: Performance of ES-FEM in Linear Elastic Analysis
Mesh Convergence in Displacement
Mesh Seed Size (m) | The Number of Triangles
1 | 22
1/2 | 84
1/4 | 342
1/8 | 1,442
1/16 | 5,766
1/32 | 23,034
1/64 | 92,146
Converged
Converged
ES-FEM-T3 is shear locking free and thus the mesh convergence rate of displacement/force is much faster than the Standard FEM-T3.
ES-FEM-T4 should also be excellent in electrostatic (ED) simulations.
Coarser
Finer

## Slide 21: Mesh Convergence Test

## Slide 22: Mesh Convergence Test
Outline
Our ED simulator, which uses FEM-T3, has been rewritten to use ES-FEM-T4.
Half-body analysis (only right-hand side).
The entire line shape, carbody motion, and electrode conditions are reproduced.
About 1000 timesteps for 300 s (i.e., average s).
The film thickness distribution is evaluated with 3 different density meshes using FEM-T4 and ES-FEM-T4.

## Slide 23: Mesh Convergence Test
Overview of Surface Mesh of 10M Element Mesh
There are many ED holes around narrow spaces among plates.
Only the surface mesh is shown.

## Slide 24: Mesh Convergence Test
Overview of Surface Mesh of 16M Element Mesh
There are many ED holes around narrow spaces among plates.
Only the surface mesh is shown.

## Slide 25: Mesh Convergence Test
Overview of Surface Mesh of 51M Element Mesh
There are many ED holes around narrow spaces among plates.
Only the surface mesh is shown.

## Slide 26: Mesh Convergence Test
Animation of Film Thickness (ES-FEM-T4 with 51M Element Mesh)
Outer View Inner View

## Slide 27: Mesh Convergence Test
Final Film Thickness Distribution on the side sill part with 51M Element Mesh
Standard FEM (FEM-T4)
Present Method (ES-FEM-T4)
Reference Solution
Standard FEM shows a little thicker result. (The center of the side sill is Yellow.)
This result is regarded as the reference solution. (The center of the side sill is Green)

## Slide 28: Mesh Convergence Test
Final Film Thickness Distribution on the side sill part with 16M Element Mesh
参照解
Standard FEM shows a much thicker result. (The center of the side sill is Orange.)
EDESFEM shows an accurate result. (The center of the side sill is Green.)
Standard FEM (FEM-T4)
Present Method (ES-FEM-T4)

## Slide 29: Mesh Convergence Test
Final Film Thickness Distribution on the side sill part with 10M Element Mesh
参照解
Standard FEM shows a massively thicker result. (The center of the side sill is Red.)
EDESFEM shows a little thicker result. (The center of the side sill is Yellow.)
A comparison of the time-history of the film thickness at this point is shown on the next page.
Standard FEM (FEM-T4)
Present Method (ES-FEM-T4)

## Slide 30: Mesh Convergence Test
Comparison of Time-histories of Film Thickness at a Sample Point on Side Sill
FEM-T4 with 51M elems. and ES-FEM-T4 with 10M elems. has almost comparable accuracy.
ES-FEM-T4 with 16M elems. gives a practically converged result.

## Slide 31: Mesh Convergence Test
Comparison of Calculation Time
On a cluster (64 CPUs: 896 cores of Intel Xeon E5-2680 v4 on TSUBAME3.0)
With the same mesh, ES-FEM-T4 is slower than FEM by x1.5.
For the same accuracy, ES-FEM-T4 is faster than FEM by x3.
# of Elements | Standard FEM (FEM-T4) | Present Method (ES-FEM-T4)
10M | 1.6 h | 1.9 h
16M | 2.3 h | 3.4 h
51M | 6.0 h | 8.5 h
Comparable Accuracy
For the simulations of actual ED lines, ES-FEM-T4 is 3 times efficient than FEM-T4.

## Slide 32: Validation Test

## Slide 33: Validation Test
●
●
●
●
●
Ch.2：Hood
Ch.4：Roof
Ch.3：Side Door
Ch.5：Side Sill
Ch.7：Back Door
Ch.6：Floor (not visible on this Fig.)
Outline
Measurement
A surface potential logging device with 6 probes was mounted on a car running on an actual ED line.
After baking, the film thickness was measured at the probe points.
Simulation (Same as the mesh convergence test.)
Half-body analysis (only right-hand side).
The entire line shape, carbody motion, and standard electrode conditions are input.
Surface potential time history and final film thickness at the 6 points are compared.
Measured 6 Points (Ch.2 - 7):

## Slide 34: Validation Test
Validation of Surface Potential (Ch. 2 and 3)
The simulated surface potential is a little high because the degradation of the membranes of electrodes was not precisely simulated; yet, the results generally agree with practical accuracy.

## Slide 35: Validation Test
Validation of Surface Potential (Ch. 4 and 5)
The simulated surface potential is a little high because the degradation of the membranes of electrodes was not precisely simulated; yet, the results generally agree with practical accuracy.

## Slide 36: Validation Test
Validation of Surface Potential (Ch. 6 and 7)
The deposition delay at the floor, an inner part, is reproduced successfully.
The simulated surface potential is a little high because the degradation of the membranes of electrodes was not precisely simulated; yet, the results generally agree with practical accuracy.

## Slide 37: Validation Test
Validation of Final Film Thickness
Point | Measured () | Simulated () | Error ()
Ch.2: Hood | 20.1 | 21.4 | 
Ch.3: Side Door | 19.0 | 21.0 | 
Ch.4: Roof | 17.0 | 19.3 | 
Ch.5: Side Sill | 20.0 | 21.6 | 
Ch.6: Floor |  | 14.5 | 
Ch.7: Back Door | 23.0 | 20.3 | 
Point |  |  | 
Ch.2: Hood | 20.1 | 21.4 | 
Ch.3: Side Door | 19.0 | 21.0 | 
Ch.4: Roof | 17.0 | 19.3 | 
Ch.5: Side Sill | 20.0 | 21.6 | 
Ch.6: Floor |  | 14.5 | 
Ch.7: Back Door | 23.0 | 20.3 | 
Although there is still room for improvement in accuracy, the maximum error in film thickness is less than 3 , which is accurate enough for practical use.

## Slide 38: Summary

## Slide 39: Summary
Electrodeposition (ED) is important for automotive safety.
Tetrahedral meshes are preferable in ED Simulation.
ES-FEM-T4 has excellent accuracy for solving Laplace equation.
In the actual line ED simulations, ES-FEM-T4 is 3 times faster than the standard FEM-T4 to obtain the same accuracy result.
The effectiveness of our ED simulator was validated by several car companies.
The application scope of ES-FEM-T4 and related FE formulations is now beginning to extend beyond Laplace simulations to solid, fluid, and acoustic simulations.
If you are interested in our ED simulator, please check the website.
Thank you for your kind attention!
Search
edesfem