## Slide 1: Electrodeposition Simulation with Edge-based Smoothed Finite Element Method using 4-node Tetrahedral Elements for Complex Car Body Shapes
Kai KITAMURA, Yuki ONISHI, Kenji AMAYA
Tokyo Institute of Technology (Japan)

## Slide 2: What is electrodeposition (ED) ?
Most widely-used basecoat methods for car bodies.
Making coated film by applying direct electric current in a paint pool.
Relatively good at making uniform film thickness but not satisfactory uniform in actual production lines.
ED simulator is necessary for optimizing carbody design and line coating conditions.
+
-
Cathode
Anode
Paint
＋
＋
http://n-link.nissan.co.jp/NOM/PLANT/

## Slide 3: Mechanism of Electrodeposition
Paint ions have positive (+) charge.
The vicinity of the cathode has negative (-) charge because of generated by electrolysis of water.
Some of the paint particles diffuse and dissolve.
-
+
+
-
Paint Ions
Carbody
（Cathode)
-
-
+
Deposition
Aggregated into paint particles
When the particle gets big enough
Power on
Coated
Film

## Slide 4: How to Develop an ED Simulator
Experiments at lab in various coating conditions.
Identification of ED boundary model and its parameters.
Implementation to a FE code.
One-Plate Test
ED simulation for actual lines
Plate
Paint
Anode
Stir bar
Plate

## Slide 5: Two Issues in Previous Studies
Coating conditions in lab experiments are different from those in actual lines.
e.g.)
Accuracy is insufficient in low voltage cases. Poor accuracy on inner surfaces of carbodies.
Lab Exp. Actual Line
The conventional lab experiments did not reproduce the actual line condition.
The conventional ED constitutive model was too simple to reproduce the complex ED phenomena.

## Slide 6: Objective
Table of body contents:
Our new Lab Experiment Method
Our new ED Boundary Model
Our S-FEM Code for ED Simulation
Validation & Demonstration Results
Propose a new lab experiment method to reproduce coating conditions of actual ED lines.
Propose a new ED boundary model to improve the accuracy of an ED simulation.

## Slide 7: Our New Lab Experiment Method

## Slide 8: Outline of the One-Plate Test
Paint
Cathode plate
Anode pot
Stirring using a stirrer
Use a rectangular steel plate instead of a car body.
Use a SS pot instead of the paint pool and anode electrodes.

## Slide 9: Outline of the One-Plate Test
Paint
Cathode plate
Anode pot
Stirring using a stirrer
Dip a steel plate into the paint pot.
Apply voltage up to 270 V between the plate and pot.
Measure time-histories of
  applied voltage,
  current
  film thickness.

## Slide 10: Our New Lab Experiment Method
Issue in the conventional lab experiment
IR drop in solution is too small.
In an actual line, IR drop in solution is about 100 V at most; however, in the conventional lab experiment, that is only 10 V.
Modification in the new lab experiment
An external resistor is introduced.
External
Resistor
Anode
Stir bar
Plate
Scale effect is canceled by the external resistor.

## Slide 11: Our New Lab Experiment Method
Comparison of Surface Potential on Cathode
ED boundary models should be identified with the new lab experiment data.
Our new lab experiment succeeded in reproducing the actual line condition.
Our new meth.
An actual line
Conventional meth.

## Slide 12: Our New ED Boundary Model

## Slide 13: Our ED Boundary Model
The governing equation in paint is the electrostatic Laplace equation ().
The difficulty in ED simulation arises on boundaries.
Our ED boundary model consists of 2 sub-models:
  Film growth model Film growth rate is NOT linear to current density : , where is a constant. It should be like
  .
  Film resistance model Film resistance is NOT linear to film thickness : , where is a constant. It should be like
  .

## Slide 14: Procedure to Identify Film Growth Model
1. One-plate tests
Plot
Data fitting
2. Scatter diagram of
3. Approximated surface

## Slide 15: Procedure to Identify Film Resistance Model
1. One-plate tests
Plot
Data fitting
2. Scatter diagram of
3. Approximated surface

## Slide 16: Our S-FEM Code for ED Simulation

## Slide 17: Our S-FEM Code for ED Simulation
What is ES-FEM-T4?
A kind of strain smoothing method.
Using element edges as Gauss points.
Robust against element skew.
Superlinear convergence rate with T4 mesh.
We adopt the edge-based S-FEM using
4-node Tetrahedral Elements（ES-FEM-T4）．
ES-FEM-T4 is always more efficient than FEM-T4.

## Slide 18: Our S-FEM Code for ED Simulation
Why not FEM-T10 but ES-FEM-T4?
T10 mesh generally requires more large number of nodes than T4 mesh to represent a complex shape.
Kinked T10 element causes severe accuracy loss.
Only surface
mesh is shown.
Provided by SUZUKI Motor Co.
ES-FEM-T4 is always more practical than FEM-T10.
 Skewed T4 (acceptable)
✗Kinked T10 (unacceptable)

## Slide 19: Validation & Demonstration Results

## Slide 20: One-plate Test
Outline
The most basic lab experiment.
500 external resistor is considered.
Simulation results are compared to experiment data.

## Slide 21: One-plate Test
Comparison of time history of film thickness
Our new ED simulator succeeded in reproducing experimental results with high accuracy from high voltage to low voltage.

## Slide 22: 4-Plate BOX Test
Outline
Imitating a multiple bag-like structure.
Accuracy on the innermost surface (left side in Figs) is the most important; i.e., “maximize the minimum”.
Objective is to confirm the validity of the ED boundary model identified with the one-plate data.

## Slide 23: 4-Plate BOX Test
Comparison of film thickness on the innermost surface
Our new ED simulator has sufficient accuracy to predict the film thickness on the innermost surface.

## Slide 24: Carbody Analysis (Outline)
Demonstration analysis.
A half carbody in a box pool.
No motion.
3M nodes, 13M elements, and 18M edges for ES-FEM-T4.
1800 time-steps for 180 s.

## Slide 25: Carbody Analysis (Film Thickness)

## Slide 26: Carbody Analysis (Surface Potential)

## Slide 27: Carbody Analysis (Current Density)

## Slide 28: Summary

## Slide 29: Summary
A new ED lab experiment method with external resistor to reproduce the actual line conditions was proposed.
A new ED boundary model considering more complex nonlinear relations was proposed.
ES-FEM-T4 was introduced in order to improve the accuracy of our ED simulator using T4 mesh.
Our new ED simulator improved the accuracy in lab tests (one-plate test & 4-plate box test).
Validation on an actual line is our issue in the future.
Thank you for your kind attention.

## Slide 30
Appendix

## Slide 31: Photos of ED process line
1. dipping and deposition process
2. water rinse process
3. baking process
We focus on this.

## Slide 32: Film Resistance Model
Model Function for Film Resistance Model
With Stirring
(1)
Without Stirring
(2)
means model parameters．
Exp.
Approx.
Exp.
Approx.