## Slide 1: Performance Evaluation of Edge-Based Smoothed Finite Element Method for 4-node Tetrahedral Meshes on Electrodeposition Simulation
Kai KITAMURA(1), Yuki ONISHI(1), Takeshi KASHIYAMA(2),
Kenji AMAYA(1)
(1) Tokyo Institute of Technology (Japan)
(2) SUZUKI MOTOR CORPORATION (Japan)

## Slide 2: What is electrodeposition (ED) ?
Most widely-used basecoat methods for car bodies.
Making coated film by applying direct electric current in a paint pool.
Relatively good at making uniform film thickness but not satisfactory uniform in actual production lines.
ED simulator is necessary for the optimization of carbody design and coating conditions in actual lines.
+
-
Cathode
Anode
Paint
＋
＋
http://n-link.nissan.co.jp/NOM/PLANT/

## Slide 3: Photos of ED process line
1. dipping and deposition process
2. water rinse process
3. baking process
We focus on this process.

## Slide 4: Mechanism of Electrodeposition
Positively charged paint ions are attracted to the cathode.
Paint ions lose their electrical charge and are aggregated into paint particles.
Some of the paint particles diffuse and dissolve.
-
+
+
-
Paint Ions
Carbody
（Cathode)
-
-
+
Deposition
Aggregated into paint particles
When the particle gets big enough
Voltage is applied
Coated
Film
Electrophoresis

## Slide 5: What is ED Simulation ?
ED simulation provides film thickness, surface potential, surface current density and so on.
Film Thickness
Surface Potential
Surface Current Density
You can see that the paint film starts to be deposited from the outside surface.

## Slide 6: How to Develop an ED Simulator
Experiments at lab in various coating conditions.
Identification of ED boundary model and its parameters.
Implementation to a FE code.
One-Plate Test
ED simulation for actual lines
Plate
Paint
On the analogy of solid mechanics,
Step 1: material tests with MTS, Step 2: identification of elastoplastic model.
DELIGHT web page, https://delightcfd.com

## Slide 7: Issues in Meshing (1)
✗ It is difficult to discretize complex shapes such as car bodies with hexahedral meshes.
→ We have to use tetrahedral meshes in ED simulation.
However…
Only surface
mesh is shown.

✗
Accuracy of the standard FEM-T4 is insufficient in complex shapes.

## Slide 8: Issues in Meshing (2)
✗ 10-node tetrahedral (T10) mesh without kink generally requires more large number of nodes than T4 mesh.
T4 T10 without kink
For the same shape representation, T10 mesh without kink leads to massive increase in DOF.
Carbody
Carbody
hole
hole

## Slide 9: Issues in Meshing (2 Cont.)
✗ 10-node tetrahedral (T10) mesh with kink causes severe accuracy loss.
T4 T10 with kink
T10 mesh with kink does not increase DOF but induces severe accuracy loss.
Carbody
Carbody
hole
hole
Kinked T10

## Slide 10: Motivation
Hexahedral elements: ✗ It is difficult to discretize complex shapes.
T10 elements without kink: ✗ It leads to massive increase in DOF.
T10 elements with kink: ✗ It causes severe accuracy loss.
→ We want to realize high accuracy analysis with T4 mesh.
ES-FEM-T4 could be a solution to these issues.

## Slide 11: Objective
Table of body contents:
Outline of ED Simulation
Formulation of ES-FEM for ED Simulation
Analysis Results
Development of ED simulator using ES-FEM-T4 and its performance evaluation by comparing with FEM-T4.

## Slide 12: Outline of ED Simulation

## Slide 13: Fundamental Equations
Governing equation
The electrostatic Laplace equation , in the paint pool domain.
Boundary conditions (BCs)
Insulation BC
Anodic (Electrode surface) BC
Cathodic (Carbody surface) BC
ED boundary models are identified with experimental data at a laboratory.
Solving the Laplace equation for potential, the current density distribution on a carbody is determined and then the film thickness distribution is time-evolutionally calculated.
+
-
Cathode
Anode
Paint
＋
＋

## Slide 14: Two Complexities of ED Phenomena
Two nonlinearities in ED boundary model
Our ED boundary model consists of 2 sub-models:
  Film resistance model Film resistance is NOT linear to film thickness :
: resistance, : const., : film thickness.
  Film growth model Film growth rate is NOT linear to current density :
: film growth rate, : const., : current density.

## Slide 15: Procedure to Identify Film Resistance Model
1. One-plate tests
Plot
Data fitting
2. Scatter diagram of
3. Approximated surface

## Slide 16: Procedure to Identify Film Growth Model
1. One-plate tests
Plot
Data fitting
2. Scatter diagram of
3. Approximated surface
Diffusive current density represents the amount of electricity consumed for the electrolysis of water, not used for the deposition of the coating film.

## Slide 17: Formulation of ES-FEM for ED Simulation

## Slide 18: Outline of ES-FEM
What is ES-FEM-T4?
A kind of strain smoothing method.
Using element edges as Gauss points.
Robust against element skew.
Super-linear mesh convergence rate with T4 mesh.
Standard FEM ES-FEM
Integration domain
Element
Node
FEM assembles each element’s value.
ES-FEM assembles each edge’s value.
Integration domain is different !!

## Slide 19: Outline of ES-FEM
Short edges
When meshing complex shape, the generation of short edges is inevitable.
Short edges lead to accuracy loss in standard FEM-T4.
Conventional FEM ES-FEM
ES-FEM can suppress the accuracy loss by smoothing.

## Slide 20: Analysis Results

## Slide 21: 4-Plate BOX Simulation
Outline
Imitating a bag-like structure such as side sill in a carbody.
Accuracy on the innermost surface (leftmost plate surface) is the most important; i.e., “maximize the minimum”.
Film thickness is calculated with 4 different mesh seed sizes and compared between FEM-T4 and ES-FEM-T4.
Film Thickness
(http://plaza.rakuten.co.jp/heroc)
Side Sill
4-P BOX

## Slide 22: 4-Plate BOX Simulation
Overview of Meshes
3.2 mm Mesh Seed Size (31k T4 elem.)
0.8 mm Mesh Seed Size (169k T4 elem.)
1.6 mm Mesh Seed Size (65k T4 elem.)
0.4 mm Mesh Seed Size (716k T4 elem.)
Only the surface meshes are shown.

## Slide 23: 4-Plate BOX Simulation
Film Thickness of A-Plate (outermost surface)
FEM results (dashed lines) have tiny errors due to mesh coarseness. Meanwhile, ES-FEM (solid lines) results have no such errors.
Mesh seed size
Notes: This graph shows the film thickness of A-Plate, which is the outermost surface.
The dashed lines show the FEM results, while the solid lines show the ES-FEM results.
As you can see, FEM results have tiny errors due to mesh coarseness.
Meanwhile, ES-FEM results have no such errors.

## Slide 24: 4-Plate BOX Simulation
Film Thickness of C-Plate (surface in the 1st bag)
FEM results (dashed lines) have small errors due to mesh coarseness. Meanwhile, ES-FEM (solid lines) results have no such errors.
Mesh seed size
Notes: This graph shows the film thickness of C-Plate which is a surface in the 1st bag.
The error is bigger than A-Plate due to mesh coarseness.

## Slide 25: 4-Plate BOX Simulation
Film Thickness of E-Plate (surface in the 2nd bag)
FEM results (dashed lines) have medium errors due to mesh coarseness. Meanwhile, ES-FEM (solid lines) results have no such errors.
Mesh seed size
Notes: This graph shows the film thickness of E-Plate which is a surface in the 2nd bag.
The error is bigger than C-Plate due to mesh coarseness.

## Slide 26: 4-Plate BOX Simulation
Film Thickness of G-Plate (innermost surface)
Mesh seed size
FEM results (dashed lines) have large errors due to mesh coarseness. Meanwhile, ES-FEM (solid lines) results have no such errors.

## Slide 27: 4-Plate BOX Simulation
Error of Final Film Thickness on G-Plate
ES-FEM-T4 has far better mesh convergence rate than FEM-T4 !!
The result of ES-FEM with the minimum mesh seed size (0.4 mm) is used as the reference.

## Slide 28: Carbody Simulation
Outline
A half carbody is fixed in a box pool.
The side wall is treated as an anode surface.
Compare the time-developed film thickness between FEM-T4 and ES-FEM-T4 with a same mesh.
270 V
0 30 180 (s)

## Slide 29: Carbody Simulation
Overview of Surface Mesh
13M T4 elements (3M nodes & 18M edges) in total in the pool.
Provided by SUZUKI MOTOR Co.

## Slide 30: Carbody Simulation
Outer View
There is no mush difference on the outer surfaces.
FEM-T4
ES-FEM-T4

## Slide 31: Carbody Simulation
Clipped View on Side Sill
Big difference appears on the inner surfaces.
As the 4-P BOX case, ES-FEM-T4 presents thinner dist. on the side sill.
FEM-T4
ES-FEM-T4

## Slide 32: Comparison of Computational Costs
Calculation Time
on a PC with Intel i9-9960X using 10 cores
 | FEM-T4 | ES-FEM-T4
4-P BOX with 3.2 mm mesh | 0.02 h | 0.02 h
4-P BOX with 1.6 mm mesh | 0.04 h | 0.05 h
4-P BOX with 0.8 mm mesh | 0.45 h | 0.45 h
4-P BOX with 0.4 mm mesh | 9.5 h | 9.0 h
Carbody | 67 h | 125 h
There is no big difference in calculation time although the accuracy of ES-FEM-T4 is much better.
Same Accuracy

## Slide 33: Summary

## Slide 34: Summary
Conclusion
ES-FEM-T4 was applied to ED simulations.
High accuracy of ES-FEM-T4 because of its super-linear mesh convergence rate was confirmed in comparison to the poor accuracy of FEM-T4.
Future Works
Validation of the ED models on the actual manufacturing lines.
Calculation speed-up with distributed memory parallelization.
Thank you for your kind attention.

## Slide 35
Appendix

## Slide 36: ED Boundary Models
Film Growth Model
It represents the relation between ．
Used to decide film growth rate.
After deposition ：
Film Resistance Model
It represents the relation between ．
Used to decide film resistance.
Flow rate dependency is considered．

## Slide 37: Comparison of Computational Costs
This is because …
Most of the calculation time is consumed by the iterative matrix solver (MINRES with Jacobi preconditioner).
The matrix band width of ES-FEM-T4 is 3 times wider than that of FEM-T4; i.e., ES-FEM-T4 requires 3 times larger memory size.
However, the iteration count of MINRES in ES-FEM-T4 is about 1/3 or 2/3 of that in FEM-T4 thanks to the well-posedness of the matrix.

## Slide 38: Carbody Simulation
Surface Current Density
FEM-T4 ES-FEM-T4
ES-FEM suppresses the spike error of surface current density appearing in FEM.

## Slide 39: Carbody Simulation
Surface Current Density
FEM-T4 ES-FEM-T4
ES-FEM suppresses the spike error of surface current density appearing in FEM.

## Slide 40: Carbody Simulation
Surface Current Density
FEM-T4 ES-FEM-T4
ES-FEM suppresses the spike error of surface current density appearing in FEM.