## Slide 1: Application of Edge-based Smoothed Finite Element Method to Electrodeposition Simulation aiming for Super-linear Mesh Convergence in Film Thickness Accuracy
Yuki ONISHI (Tokyo Institute of Technology)

## Slide 2: What is Electrodeposition (ED) ?
Most widely-used anti-rust basecoat methods for various metal products including auto carbodies.
Depositing coating film by applying direct electric current in a paint pool.
Relatively good at depositing a uniform film on bodies in complex shapes.
Cathode
Anode
Paint
＋
http://n-link.nissan.co.jp/
＋

## Slide 3: What is Electrodeposition (ED) ?
Overview of the Carbody Paint Shop
ED Oven
Degrease
Intermediate Oven
Intermediate Coat
Topcoat Oven
Top Coat
To Assembly Line
Sealing/Undercoat
Electrodeposition (ED)
Preparation
ED is responsible for the basecoat of a carbody.

## Slide 4: What is Electrodeposition (ED) ?
Photos of ED Process Line
1. Deposition process
2. Water rinse process
3. Baking process
We focus on this process.
https://blog.mazda.com/archive/20160413_01.html

## Slide 5: What is ED Simulation?
Actual ED Line
ED Simulation
Electrodes (Anodes)
Paint Pool
Carbody w/ Motion
Total length: about 30 m
Paint Pool
Carbody with Motion
Electrodes (Anodes)
are reproduced in a computer.
Paint Pool Mesh
Carbody Mesh
are separately prepared and are connected with the overset mesh method.
https://blog.mazda.com/ archive/20160413_01.html

## Slide 6: What is ED Simulation?
Outputs: time-histories of
  Surface potential,
  Current density,
  Film thickness
Final film thickness is the main output.
Governing equation: Electrostatic Laplace equation () in the paint pool domain.
A paint pool mesh and carbody meshes are connected with the overset mesh method.
Boundary conditions:
  Wall (insulation) BC，
  Anodic (electrode surface) BC,
  Cathodic (carbody surface) BC: Film resistance/growth constitutive model (Strongly non-linear).
Identified via lab experiments.

## Slide 7: Motivation
The actual ED line simulations cost high due to the large number of meshes. E.g., a typical actual ED line simulation for 3 carbodies sank in a paint pool at the same time requires about 100 million elements in total.
The standard FEM with 4-node tetrahedral elements (FEM-T4) is known as a poor formulation due to the slow (linear) mesh convergence rate.
The edge-based smoothed FEM using T4 meshes (ES-FEM-T4) is known as a next-generation high-performance formulation achieving a super-linear mesh convergence rate even with T4 meshes.
Therefore, we expect that…
Parallelized ES-FEM-T4 would be the best choice for the actual ED line simulations for automakers.

## Slide 8: Objective
Table of body contents:
Two Major Reasons for “Why did we choose ES-FEM-T4?”
Implementation of Parallelized ES-FEM-T4
Benchmark Tests
Summary
Development of an ED simulator using the parallelized ES-FEM-T4 for large-scale practical ED simulations to achieve super-linear mesh convergence.

## Slide 9: Two Major Reasons for “Why did we choose ES-FEM-T4?”

## Slide 10: Why did we choose ES-FEM-T4?
Reason 1: It is impossible to make good HEX meshes for carbodies.
An ED simulation requires a mesh for the complex spaces around the carbody.
The Cartesian meshing generates unnecessarily fine meshes on curved surfaces.
TET meshes are preferable in ED simulation.
Sliced view of a carbody mesh
A CutCell mesh of a carbody

## Slide 11: Why did we choose ES-FEM-T4?
Reason 2: There are many small holes on the carbody plates.
ED simulations need 3D meshes around many ED holes.
The 10-node TET meshing for the standard 2nd –order TET elements leads to a massive increase in nodes and DOF around ED holes.
ES-FEM-T4 would be the best choice.
Side Sill
Carbody
Hole
Carbody
Hole
T4 mesh
T10 mesh
The 4-node TET (T4) meshing is preferable.
https://plaza.rakuten.co.jp/ heroc/diary/201212210000/

## Slide 12: Implementation of Parallelized ES-FEM-T4

## Slide 13: Brief Formulation of ES-FEM
Let us consider two 3-node triangular (T3) elements in 2D for simplicity.
Calculate at each element as usual.
Distribute to each connecting edge with an area weight and build .
Calculate current density and nodal internal current in each edge smoothing domain.
As if putting a Gauss point on each edge center
etc.

## Slide 14: Characteristics of ES-FEM-T4
Advantages
Super-linear mesh convergence rate (as fast as 2nd-order elements).
No increase in DOF (Unknowns are nodal potentials only).
Same input file as FEM-T4.
Disadvantages
Longer assembling time of (~x2 of FEM-T4 w/ the same mesh) ES-FEM uses edges.
Wider bandwidth of (~x3 of FEM-T4 w/ the same mesh). In 2D case:
No longer an independent T4 element (No good way to implement in standard FE codes).
FEM-T3 (Bandwidth: 7)
ES-FEM-T3 (Bandwidth: 13)
A node is used by 6 elements, 7 nodes.
A node is used by 12 edges, 12 elements, 13 nodes.
All these disadvantages are cleared by developing parallelized in-house code.

## Slide 15: Parallelization of ES-FEM-T4
Our code adopts MPI/OpenMP hybrid parallelization for multi-core CPUs in multi-node HPC environments.
In the MPI/OpenMP coding, there is no particular difference from that of FEM-T4.
Execution steps:
  Generating T4 mesh for paint pool and carbody domains.
  Partitioning and reordering each mesh using METIS.
  Preparing an input file containing the mesh filenames, boundary conditions, motion path, etc..
  Executing the program. E.g., in the case of OpenMPI: orterun –np N -bind-to socket -npersocket 1 -x OMP_NUM_THREADS=8 -x numactl -l edesfem.bin input_file_name
Paint pool mesh partitioning
Carbody mesh partitioning
There is no difficulty in parallelization of ES-FEM-T4.

## Slide 16: Parallelization of ES-FEM-T4
Review of a Typical Processing Flow in the Parallelized FEM-T3
  Partitioning assigns “nodes in charge” to each MPI process.
  Each MPI process extracts “related cells”, which use the nodes in charge.
  Each MPI process extracts “related nodes”, which are used by the related cells.
  Each OpenMP thread in an MPI process calculates the contributions of related cells and makes and for the rows of nodes in charge.
Partitioned Domain for Process 0
Nodes in Charge
Related Cells
Related Nodes
2D explanation for simplicity

## Slide 17: Parallelization of ES-FEM-T4
Brief of the Processing Flow in Our Parallelized ES-FEM-T3
  Partitioning assigns “nodes in charge” to each MPI process.
  Each MPI process extracts “related cells”, which use the nodes in charge.
  Each MPI process extracts “related edges”, which compose the related cells.
  Each MPI process updates “related cells”, which use the related edges.
  Each MPI process extracts “related nodes”, which are used by the related cells.
  Each OpenMP thread in an MPI process calculates the contributions of related edges and makes and for the rows of nodes in charge.
Partitioned Domain for Process 0
Nodes in Charge
Related Cells
Related Nodes
The number of overlapping nodes has increased compared to FEM, which leads to a slight increase in calculation and communication costs.
Related Edges
2D explanation for simplicity

## Slide 18: Benchmark Tests

## Slide 19: 4-Plate BOX Analysis
Outline
Imitating a bag-like structure such as a side sill in a carbody.
Film thickness on the innermost face (Face G) is the most important so as to guarantee corrosion protection.
The film thickness is evaluated with 4 different meshes for using FEM-T4 and ES-FEM-T4 to compare the mesh convergence rate.
Film Thickness Anim.
4 Plates forms 3 bags.
3rd bag is difficult to be deposited.
Photo of a BOX

## Slide 20: 4-Plate BOX Analysis
Overview of 4 Meshes
3.2 mm Mesh Seed Size (31k T4 elem.)
0.8 mm Mesh Seed Size (169k T4 elem.)
1.6 mm Mesh Seed Size (65k T4 elem.)
0.4 mm Mesh Seed Size (716k T4 elem.)
Only the surface meshes are shown.

## Slide 21: 4-Plate BOX Analysis
Film Thickness on Face G (innermost face)
FEM results (dashed lines) have large errors.
Mesh seed size
Meanwhile, ES-FEM results (solid lines) have no such errors due to the fast mesh convergence rate.

## Slide 22: 4-Plate BOX Analysis
Comparison of Mesh Convergence Rate on Face G (innermost face)
FEM-T4 shows a linear convergence.
ES-FEM-T4 shows a quadratic convergence.
ES-FEM-T4 has much better mesh convergence rate than FEM-T4.
The result of ES-FEM with the finest mesh (0.4 mm) is used as the reference.
In Final thickness

## Slide 23: 4-Plate BOX Analysis
Comparison of Calculation Time
on a PC (only 1 CPU: Intel i9-9960X)
With the same mesh, ES-FEM is slower than FEM by x2.
For the same accuracy, ES-FEM is faster than FEM by x4.
Mesh Size | FEM-T4 | ES-FEM-T4
3.2 mm | 7 s | 10 s
1.6 mm | 8 s | 14 s
0.8 mm | 12 s | 26 s
0.4 mm | 41 s | 125 s
Comparable Accuracy
ES-FEM-T4 is supremely efficient in comparison to FEM-T4.

## Slide 24: Actual Line Analysis
Outline
Half-body analysis (only right-hand side).
Entire line shape, carbody motion, and electrode conditions are faithfully reproduced.
About 1000 timesteps for 300 s (i.e., average s).
The film thickness distribution is evaluated with 3 different density meshes using FEM-T4 and ES-FEM-T4.

## Slide 25: Actual Line Analysis
Overview of Surface Mesh of 10M Element Mesh
There are many ED holes around narrow spaces among plates.
Only the surface mesh is shown.

## Slide 26: Actual Line Analysis
Overview of Surface Mesh of 16M Element Mesh
There are many ED holes around narrow spaces among plates.
Only the surface mesh is shown.

## Slide 27: Actual Line Analysis
Overview of Surface Mesh of 51M Element Mesh
There are many ED holes around narrow spaces among plates.
The difference in the mesh can be seen clearly by zooming in around a hole.
Only the surface mesh is shown.
Let’s zoom in here.

## Slide 28: Actual Line Analysis
Zoom in View around the Hole on Carbody
There are many ED holes around narrow spaces among plates.
The difference in the mesh can be seen clearly by zooming in around a hole.
10M
16M
51M
Coarse Fine

## Slide 29: Actual Line Analysis
Animation of Film Thickness (ES-FEM-T4 with 51M Element Mesh)
Outer View Inner View

## Slide 30: Actual Line Analysis
Final Film Thickness Distribution on the Side Sill Part with 51M Element Mesh
Standard FEM-T4
ES-FEM-T4
Reference Solution
Standard FEM-T4 shows a little thicker result. (The center of the side sill is Yellow.)
This result is regarded as the reference solution. (The center of the side sill is Green)

## Slide 31: Actual Line Analysis
Final Film Thickness Distribution on the Side Sill part with 16M Element Mesh
参照解
Standard FEM-T4 shows a much thicker result. (The center of the side sill is Orange.)
ES-FEM-T4 shows an accurate result. (The center of the side sill is Green.)
Standard FEM-T4
ES-FEM-T4

## Slide 32: Actual Line Analysis
Final Film Thickness Distribution on the Side Sill part with 10M Element Mesh
参照解
Standard FEM-T4 shows a massively thicker result. (The center of the side sill is Red.)
ES-FEM-T4 shows a little thicker result. (The center of the side sill is Yellow.)
For more qualitative comparison, the time-history of the film thickness at this point is shown on the next page.
Standard FEM-T4
ES-FEM-T4

## Slide 33: Actual Line Analysis
Comparison of Time-histories of Film Thickness at the Sample Point on the Side Sill
FEM-T4 with 51M elems. and ES-FEM-T4 with 10M elems. has almost comparable accuracy.
ES-FEM-T4 with 16M elems. gives a practically converged result.

## Slide 34: Actual Line Analysis
Comparison of Calculation Time
On a cluster (64 CPUs: 896 cores of Intel Xeon E5-2680 v4 on TSUBAME3.0)
With the same mesh, ES-FEM-T4 is slower than FEM-T4 by x1.5.
For the same accuracy, ES-FEM-T4 is faster than FEM-T4 by x3.
# of Elements | Standard FEM-T4 | ES-FEM-T4
10M | 1.6 h | 1.9 h
16M | 2.3 h | 3.4 h
51M | 6.0 h | 8.5 h
Comparable Accuracy
For the simulations of actual ED lines with parallel computing, ES-FEM-T4 is much more efficient than FEM-T4.
An actual line analysis of a single-body entry takes only a few hours.

## Slide 35: Actual Line Analysis
Strong Scaling Test (with 10M Element Mesh)
On a cluster (up to 64 CPUs: 896 cores of Intel Xeon E5-2680 v4 on TSUBAME3.0)
Our ES-FEM-T4 code scales to some extent up to 64 CPUs at least.
  Some tasks, including MPCs for the moving boundary, are not yet fully parallelized (our future work).

## Slide 36: Summary

## Slide 37: Summary
Conclusion
ES-FEM-T4 was applied to large-scale practical ED simulations.
The high accuracy of ES-FEM-T4, owing to its super-linear (almost quadratic) mesh convergence rate in ED simulation, was confirmed compared to the poor accuracy of the standard FEM-T4.
Our parallelized ES-FEM-T4 code enabled us to obtain mesh-converged accurate solutions of actual ED line simulations in reasonable time with relatively coarse meshes.
Our code is already in use by automakers.
Further improvement using the edge center-based strain smoothing element (EC-SSE-T4) is our work in the future.
For more information, please visit our commercial code “EDESFEM” official website.
Thank you for your kind attention.
Search
edesfem

## Slide 38: Appendix

## Slide 39: Actual Line Analysis
Animation of Surface Potential (ES-FEM-T4 with 51M Element Mesh)
Outer View Inner View

## Slide 40: Actual Line Analysis
Animation of Current Density (ES-FEM-T4 with 51M Element Mesh)
Outer View Inner View