## Slide 1: Performance evaluation of the edge center-based strain smoothing element with selective reduced integration using 4-node tetrahedral meshes (EC-SSE-SRI-T4) in nearly incompressible large deformation analyses
Yuki ONISHI (Tokyo Institute of Technology)

## Slide 2: Motivation
What we want to do:
Solve severe large deformation analyses accurately and robustly.
Treat complex geometries with tetrahedral meshes.
Consider nearly incompressible materials .
Support contact problems.
Handle auto re-meshing.
Rubber
Plastic/Glass
Metal

## Slide 3: Issues in Conventional FE (ABAQUS）
e.g.) Barreling of Rubber Cylinder Neo-Hookean hyperelastic body with
ABQUS C3D4H  No volumetric locking.
✗ Pressure checkerboarding.
✗ Shear locking & Corner locking.
ABAQUS C3D10MH
 No shear/volumetric locking.
✗ Short lasting (weak to severe deformation). ✗ Low interpolation accuracy.
Almost the same # of nodes.
Pressure
Pressure
4 node tet (T4)
10 node tet (T10)
T4
T10

## Slide 4: Our Approach using S-FEM
e.g.) Barreling of Rubber Cylinder Neo-Hookean hyperelastic body with
F-barES-FEM-T4 (2017)
 No shear/volumetric locking.
 Less pressure checkerboarding.  Less corner locking. Long lasting.
 No oscillation in deviatoric stress. ✗ Long CPU time. Incompatible w/ FE.
SelectiveCS-FEM-T10 (2021)
 No shear/volumetric locking.
 Less pressure checkerboarding.  Less corner locking. Long lasting. ✗ Major oscillation in deviatoric stress.  Same CPU time. Compatible w/ FE.
4 node tet (T4)
10 node tet (T10)
T4
T10
More than 10 times slower than FEM-T4, but no good idea for speed-up…
Cannot suppress
stress oscillation, but no good idea for accuracy improvement…
Pressure
Pressure

## Slide 5: Birth of a Next-gen S-FEM, EC-SSE, in 2022
Comparison of Mises stress dist. in cantilever bending analyses in 2D
T. Jinsong et al., Euro. J. Mech. /A, v95, 2022.
Step-like stress dist. (poor).
Shear locking.
Edge Center-based Strain Smoothing Element
Detailed Later
Linear stress dist. (very good) using the same T3 mesh. Very close to analytical solution.
No shear locking.
EC-SSE is an excellent formulation for compressible solids; but when , EC-SSE has volumetric locking and pressure checkerboarding. Therefore, EC-SSE is NOT directly applicable to nearly incompressible solids.
T3
Poisson’s Ratio:
This breakthrough should be called
“S-FEM 2.0”.

## Slide 6: Objective
Objective
Strategy
Use the selective reduced integration (SRI)
Use EC-SSE for the deviatoric part,
Use NS-FEM for the volumetric part, and
Combine them with SRI.
Develop a new S-FEM formulation to extend EC-SSE to nearly incompressible large deformation analysis
EC-SSE-SRI

## Slide 7: Method Introduction to ES-FEM, NS-FEM，EC-SSE，and EC-SSE-SRI

## Slide 8: Brief of ES-FEM
Let us consider a mesh with only two 3-node triangular cells.
Make at each cell as usual.
At each edge, gather s of the connecting cells and average them with area weights to build .
Calculate strain , stress () and nodal internal force in each edge smoothing domain with .
As if putting a Gauss point on each edge center
Strain distribution is piecewise constant in each smoothing domain.
No shear locking.
Cannot avoid volumetric locking & pressure checkerboarding.
Let me explain in 2D for simplicity
etc.

## Slide 9: Brief of NS-FEM
Let us consider a mesh with only four 3-node triangular cells.
Make at each cell as usual.
At each node, gather s of the connecting cells and average them with area weights to build .
Calculate strain , stress () and nodal internal force in each nodal smoothing domain with .
As if putting a Gauss point on each node center
etc.
No shar/volumetric locking. Less pressure checkerboarding
Cannot avoid spurious low-energy modes.
Let me explain in 2D for simplicity
Strain distribution is piecewise constant in each smoothing domain.

## Slide 10: Brief of EC-SSE
Make s in the same procedure as ES-FEM.
Consider each is the value at the center of each edge, and assume is linearly distributed in each cell.
Make three s in each cell as the extrapolation of the three s.
Calculate , and using each in the same manner as the 2nd -order element.
No shear locking with T3/T4 mesh.
Fast mesh convergence rate in strain/stress as an 2nd –order element.
Strain distribution is piecewise-linear in each cell and is continuing at every edge center.
Conducting strain smoothing twice, the strain/stress are evaluated at each Gauss point.
Let me explain in 2D for simplicity
Cannot avoid volumetric locking and pressure checkerboarding

## Slide 11: Brief of EC-SSE-SRI (Our Latest Method)
Apply the selective reduced integration (SRI) to EC-SSE to handle rubber-like solids
(1) Calculate at each Gauss point with EC-SSE
(3) Calculate at each node with NS-FEM
(5) Assemble
(2) Calculate at each Gauss point and its contribution to
(4) Calculate at each node and its contribution to
Selective Reduced Integration (SRI)
Let me explain in 2D for simplicity
Deviatoric strain distribution is piecewise-linear in each cell and is continuing at each edge center.
No shear/volumetric locking. Less pressure checkerboarding.
Deviatoric Part
Volumetric Part

## Slide 12: Brief of EC-SSE-SRI-T4 (in 3D)
[Deviatoric Part]
Make s in the same procedure as ES-FEM.
Make s by re-smoothing three s per face.
Consider each is the value at the center of each face, and assume is linearly distributed in each cell.
Make four s in each cell as the extrapolation of the four s.
Calculate , and using each , like the 2nd -order element.
[Volumetric Part]
Make s in the same procedure as NS-FEM.
Calculate , and using each .
[SRI]
Make .
Let me explain with text only

## Slide 13: Result & Discussion Performance evaluation of EC-SSE-SRI-T4 in 3D and Discussion of CPU Cost

## Slide 14: Bending of Rubber Cantilever
Outline
10 x 1 x 1 m cantilever.
Neo-Hookean hyperelastic material, .
Dead load applied to the tip node.
A large deflection analysis with m at the final state.
Compared the results of ABAQUS C3D4 and EC-SSE-SRI-T4.
Dead Load
Static Implicit

## Slide 15: Bending of Rubber Cantilever
Results of ABAQUS C3D4 (Final State)
Discontinuous distribution.
Volumetric locking. (-15% error in deflection)
Severe pressure checkerboarding.
Static Implicit
***WARNING: THE INITIAL BULK MODULUS OF 9.93333E+10 EXCEEDS 25 TIMES THE
INITIAL SHEAR MODULUS OF 2.00000E+09 (SO THE INITIAL POISSONS
RATIO 0.49000 EXCEEDS 0.48) FOR THE HYPERELASTIC MATERIAL NAMED
MATERIAL-1. HOWEVER, A HYBRID TYPE ELEMENT IS NOT USED. THIS MAY
CAUSE CONVERGENCE PROBLEMS.
ABAQUS dat file:

## Slide 16: Bending of Rubber Cantilever
Results of EC-SSE -SRI-T4 (Final State)
Smooth distribution.
No locking.
Little oscillation, but no checkerboarding.
Static Implicit

## Slide 17: Bending of Rubber Cantilever
Results of EC-SSE-SRI-T4 with Different s (Final State)
No major difference in the Mises stress distributions.
Major pressure checkerboarding in the case of .
Limit of proposed method: up tp .
Static Implicit

## Slide 18: Pressuring of Rubber Block
Outline
1 x 1 x 1 m block.
Arruda-Boyce hyperelastic material, GPa, .
Applying pressure on ¼ of the top face with lateral confinement.
Evaluated the result of EC-SSE-SRI-T4.
Load
Static Implicit

## Slide 19: Pressuring of Rubber Block
Results of EC-SSE-SRI-T4
No big issue in stress distributions
Sufficient large deformation robustness
Static Implicit

## Slide 20: Barreling of Rubber Cylinder
Outline
1 m cylinder in radius and height.
Neo-Hookean hyperelastic material, .
Applying enforced compression displacement on the top face with lateral confinement.
Evaluated the result of EC-SSE-SRI-T4.
Static Implicit

## Slide 21: Barreling of Rubber Cylinder
Results of EC-SSE-SRI-T4
No problem in Mises stress.
Minor oscillation in pressure.
Convergence failure at 37% compression.
Static Implicit
Within acceptable range, I think.
acceptably robust in large deformation

## Slide 22: Tensioning of Rubber-Filler Composite
Outline
0.5 x 0.5 x 0.5 m cube (1/8 model)
Rubber: Neo-Hookean hyperelastic material
Iron Filler: Neo-Hookean hyperelastic material
Applying enforced tensioning displacement on the top face with lateral confinement.
Evaluated the result of EC-SSE-SRI-T4.
Static Implicit

## Slide 23: Tensioning of Rubber-Filler Composite
Results of EC-SSE -SRI-T4
Minor pressure oscillation only in rubber part.
No issue in Mises stress.
Convergence failure at 221% stretch sufficiently robust in large deformation
Static Implicit
Within acceptable range, I think.

## Slide 24: Discussion on CPU Time of EC-SSE-SRI-T4
Since the most of CPU time for implicit analyses is spent solving the stiffness equation (i.e., ), the size of matrix () directly affects the CPU time.
EC-SSE-SRI-T4 is a purely displacement-based FE formulation; thus, the matrix size () is exactly identical to that of FEM-T4.
EC-SSE-SRI-T4 conducts strain smoothing across FE cells; thus, the matrix bandwidth of is x6.7 wider than that of FEM-T4.
Therefore, as for calculation speed, EC-SSE-SRI-T4 is about x6.7 slower than FEM-T4.
Formulation | Bandwidth of | v.s. FEM-T4 Ratio
FEM-T4 | 14 nodes x 3 DOF | 1
FEM-T10 | 28 nodes x 3 DOF | 2.0
ES-FEM-T4 | 45 nodes x 3 DOF | 3.2
NS-FEM-T4, SelectiveES/NS-FEM | 60 nodes x 3 DOF | 4.3
EC-SSE-T4, EC-SSE-SRI-T4 | 94 nodes x 3 DOF | 6.7
Formulation |  | v.s. FEM-T4 Ratio
FEM-T4 | 14 nodes x 3 DOF | 1
FEM-T10 | 28 nodes x 3 DOF | 2.0
ES-FEM-T4 | 45 nodes x 3 DOF | 3.2
NS-FEM-T4, SelectiveES/NS-FEM | 60 nodes x 3 DOF | 4.3
EC-SSE-T4, EC-SSE-SRI-T4 | 94 nodes x 3 DOF | 6.7

## Slide 25: Discussion on CPU Time of EC-SSE-SRI-T4
Meanwhile, we should remind that
  FEM-T4 cannot avoid volumetric locking and pressure checkerboarding,
  FEM-T10 cannot have large deformation robustness (short-lasting),
  no matter how fine the mesh is.
Therefore, I believe, EC-SSE-SRI-T4 is practically acceptable and worth using, even though the CPU time is 7 times longer than FEM-T4.
What do you think?

## Slide 26: Summary

## Slide 27: Summary
A next-gen S-FEM, EC-SSE-T4, was upgraded to EC-SSE-SRI-T4 to handle rubber-like materials.
The performance of EC-SSE-SRI-T4 in large deformation nearly incompressible analyses is summarized as follows:
  No shear/volumetric locking.
  Only minor pressure checkerboarding when .
  7 times longer CPU time than FEM-T4 when using the same mesh.
  More accurate than conventional T4 elements and SelectiveES/NS-FEM-T4.
  More robust (long-lasting) than conventional T10 elements.
The EC-SSE family would be the standard T4 formulation in the near future.
Thank you for your kind attention!

## Slide 28: Appendix

## Slide 29: Difference in Formulation
Strain Distribution in each Formulation
FEM and ES-FEM: Piece-wise constant, Different pieces.
SSE and EC-SSE: Piece-wise linear, Different continuity.
FEM
ES-FEM
EC-SSE
SSE
If calculation time is disregarded, EC-SSE is expected to provide highly accurate strain/stress with a T3/T4 mesh.
Let me explain in 2D for simplicity

## Slide 30: Brief of SSE
Make s in the same procedure as ES-FEM.
Consider each represents in its edge smoothing domain, and assume is linearly distributing in each cell.
Make three s in each cell as the average of neighbor two s .
Calculate , and using each in the same manner as the 2nd -order element.
Let me explain in 2D for simplicity
No shear locking with T3/T4 mesh.
Fast mesh convergence rate in strain/stress.
Strain distribution is piecewise-linear in each cell
Conducting strain smoothing twice, the strain/stress are evaluated at each Gauss point.
Cannot avoid volumetric locking and pressure checkerboarding

## Slide 31: Why not T10 but T4?
It is because T10 mesh is NOT good for the representation of complex geometries.
For example, surface mesh around a small hole looks like…
Also, the presence of mid-nodes leads to early convergence failure in large deformation.
Then, T4 is preferable.
solid
Hole
T10 mesh w/ kink
✗ leads to severe
accuracy loss.
solid
Hole
T10 mesh w/o kink
✗ leads to a massive
increase in DOF.
solid
Hole
T4 mesh
is excellent with ES-FEM
using minimal # of meshes.
T10
T4