## Slide 1: Numerical modeling method to reproduce UV imprint process using thermo-viscoelastic constitutive law
R. YAMASHITA a, Y. ONISHI a, K. AMAYA a, Y. HIRAI b
a Tokyo Institute of Technology, Japan
b Osaka Prefecture University, Japan

## Slide 2: Background
UV imprinting is a low cost and high throughput production method.
It has been adopted to the production of various optical devices requiring high surface accuracy such as micromirror array.
PDMS Mold
UV Resin
Mold
UV Exposure & Demolding
UV Resin
Example of optical product produced by micro imprint.
Parity Innovations Co., Ltd.
https://www.piq.co.jp/about_e.html

## Slide 3: Issues
In the curing process, volume shrinkage of UV resin arises and may cause unintended surface curvature when a soft mold such as PDMS is used.
There is no numerical modeling method to reproduce this type of error in UV imprint, although there are a few conventional methods for thermal imprint.
UV Resin
Soft Mold
UV Resin
Soft Mold
Shrink
UV
Exposure
Demolding
Y. Onishi et al. Jpn. J. Appl. Phys. 47 5145 (2008)
UV Resin
✘
Unintended Surface Curvature

## Slide 4: Brief of Conventional Method for Thermal Imprint Simulation
Thermo-viscoelastic constitutive model
  Thermal contraction is described with thermal expansion coefficient.
  Shear behavior is described with the time- temperature superposition principle and Prony series for the generalized Maxwell model.
  Volumetric behavior is assumed to be independent of strain rate and temperature.
Numerical simulation with the finite element method (FEM)
Ginf
Gn
1
n
G1
Our idea：
Similar numerical approach could be used for UV imprint simulation.

## Slide 5: Objective
Propose a numerical method for UV curing process simulation.
Perform a numerical analysis for validation of the proposed numerical method.

## Slide 6: Methods

## Slide 7: Overview of Our Method
Considering the analogy of thermal and UV imprint,
Our approach uses thermo-viscoelastic material constitutive model and replaces phenomena on UV resin as follows.
    UV reaction progress Cooling (temperature drop)
    UV shrink Cooling contraction
    UV curing Cooling solidification
Virtual temperature is introduced for the UV reaction progress measure.
The model parameters are identified through rheology measurement experiments.
Numerical UV process simulation is realized as the result.
Becomes similar to thermal imprint simulation

## Slide 8: Experimental Conditions
Rotational oscillatory rheometer (Anton Paar MCR301) is used.
The measurement object is a cationic polymerization-type UV resin from Daicel Co..
Room temperature is 25℃ (const.).
UV exposure condition is constant (30 s exposure in a constant intensity).
The oscillation frequency is varied from 0.1 to 10 Hz.
The gap between the cylinder rod and the glass plate changes over time due to UV shrink.
Long time measurement is conducted to consider the dark curing.
Cylinder
Rod
Glass Plate
UV Resin
UV Light
Small Rotational Oscillation
Follow
Gap
Change
Gap
0 30 time (s)
Intensity
Anton Paar MCR series
https://www.anton-paar.com/corp-en/products/details/rheometer-mcr-102-302-502/

## Slide 9: Relative Gap Change (Experimental Result)
Time History of Relative Gap Change
Note: the time history of the relative gap change is always the same in all cases (∵ UV exposure condition is constant).
UV shrink progresses with time, and the shrink speed gradually decreases.

## Slide 10: Relative Gap Change (Model Parameter Identification)
UV shrink is modeled as thermal (cooling) contraction.
The time history of virtual temperature is given as . (Note that is not a real physical quantity but just a virtual value.)
The time history of relative gap change is converted into the virtual temperature-dependent coefficient of thermal expansion.
Virtual Temperature- Dependent Coefficient of Thermal Expansion
Note: is negative because it represents the volume change compared to the initial volume.
Virtual

## Slide 11: Viscoelasticity (Experimental Result)
Time History of Storage / Loss Shear Modulus ()
Depending on the frequency, the time histories of and are different (harder at higher frequencies).
At any frequency, UV resin monotonically hardens with time.

## Slide 12: Viscoelasticity (Model Parameter Identification 1/2)
UV resin is modeled as viscoelastic material based on the time-temperature superposition principle and Prony series for the generalized Maxwell model.
The reference virtual temperature is set as .
Pick s and s at various s and identify each time shift.
Time-Shifted Storage Shear Modulus at (Master Curve)
P. 12
In practice, is also taken into consideration to determine the time shifts.
Shift for
Shift for
Shift for
Shift for
Shift for
Measurement at

## Slide 13: Viscoelasticity (Model Parameter Identification 2/2)
Find the Prony series coeffs by fitting the master curve at the reference temp.
Storage / Loss Shear Modulus at Reference Temp. Expressed by Prony Series
From the above, the constitutive model of thermo-viscoelasticity to simulate UV shrink and curing were identified.

## Slide 14: Result & Discussion

## Slide 15: UV Curing Process Simulation (Outline)
Commercial finite element code, ABAQUS, is adopted.
Target pattern is a micromirror array.
The mold pattern is periodic and thus only one pattern is taken into account with periodic boundary conditions.
Mold cavity is filled with UV resin at the initial state.
Virtual temperature is given as .
UV exposure condition is exactly the same as that of the rheology measurement experiments. (30 s exposure in a constant intensity).
Demolding is conducted 100 s after the end of UV exposure.
Curvature on top surface of UV resin is evaluated enough after the demolding (6000 s).
Top Surface
of UV Resin
PDMS Mold
UV Resin
3D View
320 m
320 m
200 m
300 m
1000 m

## Slide 16: UV Curing Process Simulation (Outline)
Commercial finite element code, ABAQUS, is adopted.
Target pattern is a micromirror array.
The mold pattern is periodic and thus only one pattern is taken into account with periodic boundary conditions.
Mold cavity is filled with UV resin at the initial state.
Virtual temperature is given as .
UV exposure condition is exactly the same as that of the rheology measurement experiments. (30 s exposure in a constant intensity).
Demolding is conducted 100 s after the end of UV exposure.
Curvature on top surface of UV resin is evaluated enough after the demolding (6000 s).
Demolding
Non-slip &
Non-separation
Contact
Periodic Boundary Condition
UV Resin
PDMS Mold
2D Cut View
Top Surface
of UV Resin

## Slide 17: UV Curing Process Simulation (Simulation Result)
Displacement Dist. in X Direction
Sectional view (cut on plane)
3D view
Right before
Demolding
Surface curvature due to the UV shrink of resin and the mold deformation is observed.
Flow of UV resin due to the UV shrink is observed.

## Slide 18: UV Curing Process Simulation (Validation)
Curvature Depth Dist. on Top Surface
Simulation Result
Experimental Result (Measured with laser microscope
VK-X100, KEYENCE Co.)
200 m
200 m
200 m
Max. depth: about 0.75
Max. depth: about 0.47
Actual
micromirror array
✔ Simulation result agreed with the experimental measurement data qualitatively.
✘ However, maximum curvature depth of simulation is smaller than experimental one.

## Slide 19: Why curvature depth of simulation is small?
Temperature time history of UV resin during UV reaction (Stage temp. ，UV intensity , 500 m thick )
Temperature time history of resin center
Recorded by thermography (FLIR C2)
UV exposure
for 30 s
Temp. drop can cause thermal contraction!
Reaction heat is quickly generated after the start of UV exposure, and the peak temperature of UV resin exceeds 100 .
Thermal contraction due to cooling should be considered.
~ 20 mm
Peak temp. at 4 s

## Slide 20: Why curvature depth of simulation is small?
Temp: low
Viscosity: low
UV shrink: yet
Temp: high
Viscosity: low
UV shrink: yet
Temp: high
Viscosity: high
UV shrink: yet
Temp: low
Viscosity: high
UV shrink: done
Mechanism of surface curvature of UV resin formed by thermal contraction (Hypothesis)
Reaction heat generated
Double Effect!?

## Slide 21: Summary

## Slide 22: Summary
A numerical modeling method for UV shrink & curing simulation using thermo-viscoelastic model was proposed.
The model parameters were identified through the rheology measurement experiments.
A process simulation for micromirror array using PDMS mold validated the qualitative accuracy on mirror surface curvature.
Our recent future works are below:
  Investigate the hypothesis to achieve the quantitative validation of our method.
  Improve our modeling method and simulation accuracy to aim for practical application.
Thank you for your kind attention.

## Slide 23: Appendix

## Slide 24: Limitation of Our Method
UV exposure condition to simulate must be exactly the same as that on the rheology measurement experiments.
The pattern size must be large enough to apply continuum approximation.

## Slide 25: Viscoelasticity (Model Parameter Identification 2/3)
A virtual temperature-dependent shift factor (i.e., time-temperature superposition) is obtained by fitting the time-shifts at various temperatures.
Virtual Temperature- Dependent Shift Factor

## Slide 26: Validation of Material Constitutive Model
Outline
Finite element analyses using the identified thermo-viscoelastic properties to reproduce the rheometer measurement data is conducted.
For simplicity, time evolution analysis that gives shear vibration to one hexahedron element is performed.
Defined thermo-viscoelastic properties are:
  Temperature-dependent coefficient of thermal expansion,
  Temperature-dependent shift factor,
  Prony series at reference temperature,
  Instantaneous Young’s modulus and Poisson's ratio
Field condition of virtual temperature is given.
Boundary conditions are:
  Perfect constraint on the lower surface
  Small oscillatory disp. in shear on the upper surface.
Small shear oscillation

## Slide 27: Validation of Material Constitutive Model
Time History of Relative Gap Change
The relative gap change is accurately simulated.

## Slide 28: Validation of Material Constitutive Model
Time History of Storage / Loss Shear Modulus
The storage shear modulus is accurately simulated. On the other hand, minor problem remains in the accuracy of the loss shear modulus because .

## Slide 29: Steps of UV Process Simulation
Step 1: Stationary (1 sec.)
  Static analysis
  Start no-slip & no-separation contact
Step 2: UV exposure & Dark curing (130 sec.)
  Quasi-static analysis
  Lower UV resin virtual temperature:
Step 3: Demolding w/ Dark curing (10 sec.)
  Quasi-static analysis
  Remove no-slip & no-separation contact
  Lift mold upward
  Lower UV resin virtual temperature:
Step 4: Dark curing (6000 sec.)
  Quasi-static analysis
  Lower UV resin virtual temperature:
Displacement 400µm
Non-slip &
Non-separation
contact
Periodic boundary condition
UV Resin
℃
PDMS Mold
ABAQUS/Standard C3D8 is used for FE analysis.

## Slide 30: Acceleration of UV reaction by reaction heat
Rheology measurement results at various stage temperature (Frequency: UV intensity: )
Relative Gap Change
The higher temperature, the faster the UV reaction.
In the actual process, UV shrink can be accelerated by the reaction heat.
Storage Shear Modulus

## Slide 31: Effect of demolding timepoint on curvature depth
Relation between demolding timepoint and max. curvature depth
Delaying the demolding timing makes the surface curvature deeper.
The more UV reaction progresses until demolding timepoint, the deeper the surface curvature.

## Slide 32: Why curvature depth of simulation is small?
In the simulation, UV shrink is not completed at the time of demolding, and the curvature depth at that time is observed.
In the actual process, UV shrink with thermal contraction has been completed before demolding, therefore the curvature depth becomes deeper than our simulation’s one.

## Slide 33: Why curvature depth of simulation is small?
Temperature time history of UV resin during UV reaction (Stage temp. ，UV intensity , 500 m thick )
Temperature time history of resin center
Recorded by thermography (FLIR C2)
UV exposure
for 30 s
~ 20 mm
Peak temp. at 15 s