## Slide 1: Identification of Paint Resistance and Deposition Model Parameters for Electrodeposition Coating Simulation
Ayaka SHIMURA, Yuki ONISHI, Kenji AMAYA
Tokyo Institute of Technology (Japan)

## Slide 2: What is electrodeposition (ED) ?
One of the popular basecoat method for car bodies.
Making coated film by passing a direct electric current.
Coated film has a certain electrical resistance, and thus
Electric current tends to flow on to thinner film areas.
(By http://www.rodip.com.br/)
Anode
Electrode
Object to Coat （Cathode）
Paint
ED is good at making coated objects with an uniform film thickness.

## Slide 3: Photos of ED process line
1. dipping and deposition process
2. water rinse process
3. baking process
We focus on this.

## Slide 4: Outline of ED mechanism
  Electric current generates and H2 from H2O on the cathode surface.
Notes: では今回新たに提案した塗膜析出モデルについて，そのイメージを説明します．
あくまでイメージですので，これが物理的に正しいのかということはわかりませんのでご注意ください．
まず，電流を流すと水の電気分解により，カソード表面でOH^−が発生し，蓄積されます．その間にOH^−の一部は拡散消費されてしまいます．

## Slide 5: Outline of ED mechanism
  Paint particle ions having positive (+) charge are attracted to toward the cathode.
paint particle
paint particle

## Slide 6: Outline of ED mechanism
  Some of the paint particle ions are neutralized and stick on the cathode surface, becoming a paint film.
カソード
カソード
paint particle
paint particle

## Slide 7: Outline of ED mechanism
  The rest of the paint particles are diffused and resolved again as ions.
  The paint film soon has a number of holes to let the next and H2 go through.
カソード
カソード
paint particle
paint particle

## Slide 8: 2 Complexities in ED phenomena
The electric resistance of the paint film is not linear with respect to the film thickness…
: resistance, : const., : film thickness.
The growth rate of the paint film is not linear with respect to the current density…
: film growth rate, : const., : current density. (These complexities in experiments are shown later in this talk.)
Experimental ED process optimization costs high! Numerical ED simulation is important.
Due to the diffusive current
Due to a number of holes

## Slide 9: Objective
Identify the two fundamental ED models,
  a nonlinear film resistance model and
  a nonlinear film growth model,
via basic ED experiments
for accurate numerical ED simulation.
Table of body contents:
Basic ED experiments
Our new models
Validation results
Summary

## Slide 10
Basic ED Experiments

## Slide 11: Outline of the one-plate test
Paint
Cathode plate
Anode pot
Stirring using a stirrer
Use a rectangular steel plate instead of a car body.
Use a SS pot instead of the paint pool and anode electrodes.

## Slide 12: Outline of the one-plate test
Paint
Cathode plate
Anode pot
Stirring using a stirrer
Dip a steel plate into the paint pot.
Apply voltage up to 250 V between the plate and pot.
Measure time-histories of
  applied voltage,
  current,
  film thickness.

## Slide 13: An example of film resistance nonlinearity
Time history of
current density
In the middle of an ED test, we changed the applied voltage quickly from
100 V to 30 V. Then, the film resistance before/after the change was estimated.
Cathodal current density, ()
Time, (s)
The film resistance should be modeled with a polarization curve depending on film thickness.
The film thickness is same, but the resistance changes quickly.
Time history of
applied voltage
Time, (s)
Applied voltage, (V)

## Slide 14: An example of film growth nonlinearity
250V
100V
50V
10V
The inclination shows the deposition efficiency.
Conventional model
Film thickness, ()
Total charge density on cathode
The film growth model should include the effect of the diffusive current depending on the voltage and film thickness.
Relation between total charge density and film thickness.
The total charge density is same, but
the deposition efficiencies are different.

## Slide 15
Our new models

## Slide 16: Procedure to identify resistance model
Plot
Data fitting
Cathode voltage drop,
()
Cathode voltage drop,
()
Cathode current density, ()
Cathode current density, ()
2. Scatter diagram of
1. One-plate tests
3. Approximated surface

## Slide 17: Procedure to identify film growth model
Plot
Data fitting
Cathode current
density, ()
Film thickness, ()
Diffusive current density, ()
Cathode current
density, ()
Film thickness, ()
Diffusive current density, ()
1. One-plate tests
2. Scatter diagram of
3. Approximated surface

## Slide 18
Validation Results

## Slide 19: Our ED simulator
In-house finite element code.
2nd order tetrahedral elements.
The experimental results of the one-plate tests are compared to the results of our simulator with the proposed nonlinear models and those with the conventional linear models.

## Slide 20: Time history of film thickness
Conventional linear models fail to represent the experimental data…
Our new nonlinear models succeeded in reproducing the experiments!
dot ：Experiment
line ：Numerical analysis
Proposed nonlinear model
Conventional linear model
Time, (s)
Time, (s)
Film thickness, ()
250V
50V
100V
10V
30V
150V

## Slide 21: Time history of current density
Numerical analysis
Experiment
Time, (s)
Time, (s)
Cathode current density, ()
Conventional linear models fail to represent the experimental data…
Our new nonlinear models succeeded in reproducing the experiments!
Proposed nonlinear model
Conventional linear model

## Slide 22
Summary

## Slide 23: Summary
A new nonlinear film resistance model and film growth model for accurate electrodeposition (ED) simulation were proposed.
The model parameters were identified via the one-plate ED tests.
Our new models improved the accuracy in time histories of the film thickness and current density compared to the conventional linear models.
Thank you for your kind attention.