## Slide 1: Application of Edge-based Smoothed Finite Element Method to Large-scale Electrodeposition Simulation for Automobile Manufacturing Lines
Yuki ONISHI Tokyo Tech. (Japan)

## Slide 2: What is Electrodeposition (ED) ?
Outline
Most widely-used anti-rust basecoat methods for various metal products including carbodies.
Depositing coating film by applying direct electric current in a paint pool.
Relatively good at depositing a uniform film on bodies in complex shape.
+
-
Cathode
Anode
Paint
＋
http://n-link.nissan.co.jp/
＋

## Slide 3: What is Electrodeposition (ED) ?
Photos of ED Process Line
1. Deposition process
2. Water rinse process
3. Baking process
We focus on this process.
https://blog.mazda.com/archive/20160413_01.html

## Slide 4: Difficulty in ED for Carbodies
Undercarriages are exposed to severe corrosive environments, especially due to seawater or snow-melting chemicals.
Some undercarriage parts (such as a side sill) have bag-like complex structures with many ED holes.
It is not easy to deposit a required minimal thick film at the innermost faces of a bag-like structure, even for ED.
Carbody design must consider the difficulty in ED process.
Side Sill
https://www.goauto.ca/

## Slide 5: What is ED Simulation?
Actual ED Line
ED Simulation
Electrodes (Anodes)
Paint Pool
Carbody w/ Motion
Total Length: about 30 m
Paint Pool
Carbody with Motion
Electrodes (Anodes)
are reproduced in a computer.

## Slide 6: What is ED Simulation?
Governing Equation: Electrostatic Laplace equation () in the paint pool domain.
Boundary Condition (BC):
  Insulation BC,
  Anodic (electrode surface) BC,
  Cathodic (carbody surface) BC: Film resistance/growth constitutive model.
Outputs:
  Surface potential,
  Current density,
  Coated film thickness. (main result)

## Slide 7: Issue 1
Issue 1: Impossible to make a good HEX mesh for carbodies.
An ED simulation requires a mesh for the space around the carbody, just like CFD.
In contrast to CFD, an ED mesh includes the room space and many narrow spaces among plates (such as side sills).
Sliced view of a carbody mesh

## Slide 8: Issue 1 (cont.)
The shape of a carbody is too complex to be discretized into a good HEX mesh.
The Cartesian meshing (cutcell or snappy HEX meshing) is basically not suitable for the geometry with many holes. ( Massive increase in DOF, Linear mesh convergence rate, Presence of hanging nodes or polyhedral cells, Inapplicable to solid dynamics, etc.)
TET meshes are preferable in ED simulation.
Zoom-in view of a carbody mesh
T4 mesh
Cutcell mesh
Only the surface mesh is shown.

## Slide 9: Issue 2
Issue 2: Both the standard 4-node and 10-node tetrahedral elements are inconvenient for carbodies.
4-node TET (T4) has poor accuracy with only a linear mesh convergence rate. FEM-T4 and FVM-T4 require very fine meshes to obtain accurate results.
10-node TET (T10) has good accuracy with a quadratic mesh convergence rate; however, T10 mesh requires massively large DOF to represent complex shapes without any kink of element shapes.

## Slide 10: Issue 2 (cont.)
For example, if there is a small hole on a carbody, the surface mesh around the hole looks like…
✗ T10 w/ kink leads to severe accuracy loss.
✗ T10 w/o kink leads to a massive increase in DOF.
Carbody
Carbody
Hole
Hole
Carbody
Hole
T4 mesh
T10 mesh w/ kink
T10 mesh w/o kink
The standard T4 and T10 elements are both inconvenient for carbodies to achieve accurate simulation with minimal DOF.

## Slide 11: Motivation
By the way, …
The smoothed finite element method (S-FEM) has become popular in recent years as a next-generation high-performance FEM.
Especially, the edge-based S-FEM using T4 mesh (ES-FEM-T4) is known to achieve a superlinear mesh convergence rate even with T4 meshes.
Therefore, we expect that…
ES-FEM-T4 could be a solution for the meshing issues to achieve fast and accurate ED simulation.

## Slide 12: Objective
Table of body contents:
Brief of ED Formulation using ES-FEM-T4
Benchmark Analyses
Summary
Development of ED simulator using ES-FEM-T4 for large-scale ED simulations of actual manufacturing lines.

## Slide 13: Brief of ED Formulation using ES-FEM-T4

## Slide 14: Brief Formulation of ES-FEM
Let us consider two 3-node triangular (T3) elements in 2D.
Calculate at each element as usual.
Distribute to each connecting edge with an area weight and build .
Calculate current density and nodal internal current in each edge smoothing domain.
As if putting an integration point on each edge center
etc.

## Slide 15: Characteristics of ES-FEM-T4
Advantage
Superlinear mesh convergence (as fast as 2nd-order elems.).
Same input file as FEM-T4.
No increase in DOF (nodal potentials only; easy to code).
Disadvantage
Longer assembling time of (~x2 of FEM-T4 w/ the same mesh).
Wider bandwidth of (~x3 of FEM-T4 w/ the same mesh).
No longer an independent T4 element.
FEM-T3 (Bandwidth: 7)
ES-FEM-T3 (Bandwidth: 13)
A node is referred by 6 elements, 7 nodes.
A node is referred by 12 edges, 12 elements, 13 nodes.

## Slide 16: Handling of Moving Boundary
The overset mesh method is adopted using two meshes (i.e., pool mesh and carbody mesh).
Each interfacial node of the active pool elements is tied in the active body elements with the multi-point constraint (MPC).
The classical method of Lagrange multiplier is used to satisfy the MPCs.
Inactive Elements
Active Body Elements
Active Pool Elements
Liquid Level

## Slide 17: Parallelization of ES-FEM-T4
There is no particular difference from FEM-T4 using MPI.
The only difference is the number of overlapping nodes, which leads to a slight increase in communication cost.
Calculation steps:
  Generating T4 mesh for pool and body domains.
  Partitioning and reordering each mesh with METIS.
  Preparing an input file containing the mesh filenames, boundary conditions, motion path, etc..
  Executing the program. (e.g., in case of OpenMPI: orterun –np N -bind-to socket -npersocket 1 -x OMP_NUM_THREADS=8 -x numactl -l edesfem.bin input_file_name)
There is no difficulty in parallelization of ES-FEM-T4.
Pool mesh partitioning
Body mesh partitioning

## Slide 18: Benchmark Analyses

## Slide 19: 4-Plate BOX Simulation
Outline
Imitating a bag-like structure such as a side sill in a carbody.
Film thickness on the innermost surface (Face G) is the most important so as to guarantee corrosion protection.
The film thickness is evaluated with 4 different meshes for mesh validation using FEM-T4 and ES-FEM-T4.
Film Thickness Anim.
4 Plates forms 3 bags.
3rd bag is difficult to be deposited.
Photo of a BOX

## Slide 20: 4-Plate BOX Simulation
Overview of Meshes
3.2 mm Mesh Seed Size (31k T4 elem.)
0.8 mm Mesh Seed Size (169k T4 elem.)
1.6 mm Mesh Seed Size (65k T4 elem.)
0.4 mm Mesh Seed Size (716k T4 elem.)
Only the surface meshes are shown.

## Slide 21: 4-Plate BOX Simulation
Film Thickness on Face G (innermost surface)
FEM results (dashed lines) have large errors.
Mesh seed size
Meanwhile, ES-FEM results (solid lines) have no such errors due to the fast mesh convergence rate.

## Slide 22: 4-Plate BOX Simulation
Comparison of Mesh Convergence Rate on Face G
FEM-T4 shows a linear convergence.
ES-FEM-T4 shows a quadratic convergence.
ES-FEM-T4 has much better mesh convergence rate than FEM-T4.
The result of ES-FEM with the finest mesh (0.4 mm) is used as the reference.
In Final thickness

## Slide 23: 4-Plate BOX Simulation
Comparison of Calculation Time
on a PC (only 1 CPU: Intel i9-9960X)
With the same mesh, ES-FEM is slower than FEM by x2.
For the same accuracy, ES-FEM is faster than FEM by x4.
Mesh Size | FEM-T4 | ES-FEM-T4
3.2 mm | 7 s | 10 s
1.6 mm | 8 s | 14 s
0.8 mm | 12 s | 26 s
0.4 mm | 41 s | 125 s
Comparable Accuracy
ES-FEM-T4 is supremely efficient in comparison to FEM-T4.

## Slide 24: Actual Line Simulation
Outline
Half-body analysis (only right-hand side).
Entire line shape, carbody motion, and electrode conditions are faithfully reproduced.
About 1000 timesteps for 300 s (i.e., average s).
The film thickness is evaluated with 3 different meshes for mesh validation using FEM-T4 and ES-FEM-T4.

## Slide 25: Actual Line Simulation
Overview of Surface Mesh of 10M Element Mesh
There are many ED holes around narrow spaces among plates.
Only the surface mesh is shown.

## Slide 26: Actual Line Simulation
Overview of Surface Mesh of 16M Element Mesh
There are many ED holes around narrow spaces among plates.
Only the surface mesh is shown.

## Slide 27: Actual Line Simulation
Overview of Surface Mesh of 51M Element Mesh
There are many ED holes around narrow spaces among plates.
The difference in the mesh can be seen clearly by zooming in around a hole.
Only the surface mesh is shown.
Let’s zoom in here.

## Slide 28: Actual Line Simulation
Zoom in View around a Hole on Carbody
There are many ED holes around narrow spaces among plates.
The difference in the mesh can be seen clearly by zooming in around a hole.
10M
16M
51M
Coarse Fine

## Slide 29: Actual Line Simulation
Animation of Film Thickness (ES-FEM with 51M Elems.)
Outer View Inner View

## Slide 30: Actual Line Simulation
Film Thickness Distribution with 51M Elem. Mesh
(Clipped View on Side Sill)
FEM shows a little thicker result. (The center of the side sill is Yellow.)
The ES-FEM result is regarded as a reference solution. (The center of the side sill is Green.)
FEM-T4
ES-FEM-T4
Reference Solution

## Slide 31: Actual Line Simulation
Film Thickness Distribution with 16M Elem. Mesh
(Clipped View on Side Sill)
FEM shows a much thicker result. (The center of the side sill is Orange.)
ES-FEM shows a similar result. (The center of the side sill is Green.)
FEM-T4
ES-FEM-T4

## Slide 32: Actual Line Simulation
Film Thickness Distribution with 10M Elem. Mesh
(Clipped View on Side Sill)
FEM shows a massively thicker result. (The center of the side sill is Red.)
ES-FEM shows a little thicker result. (The center of the side sill is Yellow.)
FEM-T4
ES-FEM-T4
Hard to be deposited but important point for anti-corrosion.
Let’s compare the time history of film thickness at a certain point.

## Slide 33: Actual Line Simulation
Comparison of Time-histories of Film Thickness
FEM-T4 with 51M elems. and ES-FEM-T4 with 10M elems. has almost comparable accuracy.
ES-FEM-T4 with 16M elems. almost gets a converged result.

## Slide 34: Actual Line Simulation
Comparison of Calculation Time
On a cluster (TSUBAME3.0: Intel Xeon E5-2680 v4, using 64 CPUs)
With the same mesh, ES-FEM is slower than FEM by x1.5.
For the same accuracy, ES-FEM is faster than FEM by x3.
# of Elements | FEM-T4 | ES-FEM-T4
10M | 1.6 h | 1.9 h
16M | 2.3 h | 3.4 h
51M | 6.0 h | 8.5 h
Comparable Accuracy
For the accurate simulations of actual ED lines, ES-FEM-T4 is much better than FEM-T4.

## Slide 35: Actual Line Simulation
Strong Scaling Test (with 10M Elem. Mesh)
On a cluster (TSUBAME3.0: Intel Xeon E5-2680 v4)
  Some tasks, including MPCs for the moving boundary, are not yet fully parallelized (our future work).
Our ES-FEM code scales to some extent up to 64 CPUs at least.

## Slide 36: Summary

## Slide 37: Summary
Conclusion
ES-FEM-T4 was applied to large-scale practical ED simulations.
The high accuracy of ES-FEM-T4, owing to its superlinear (almost quadratic) mesh convergence rate in ED simulation, was confirmed compared to the poor accuracy of FEM-T4.
Our parallelized ES-FEM-T4 code enabled us to obtain mesh-converged accurate solutions of actual ED line simulations in reasonable time with relatively coarse meshes.
Our code is already in use by automakers.

## Slide 38: Summary
Acknowledgment We appreciate the automakers below for supporting our project:
SUZUKI Motor Corp., SUBARU Corp., MAZDA Motor Corp..
Take-home Message
Why don’t you use ES-FEM-T4? It’s supremely useful and easy to code!
Thank you for your kind attention.